## Slide 1
Single-chain polymer nanoparticles via reversible disulfide bridges
Introduction:
In analogy to nature, the fabrication of functional nanodevices from well-defined discrete macromelecules remains an important yet elusive research objective. Single-chain polymer nanoparticles (SCNPs) represent a significant step towards these ends. This technique is predicated on the concept that in sufficiently dilute polymer solutions (concentrations below the overlap concentration, c*), inter-chain interactions are minimized because the dimenstions of individual chains are smaller than the average distance between the chains. Thus, triggering a cross-linking reaction under these conditions will result in intrachain, rather than interchain coupling, facilitating a change in conformation from an expanded coil to a collapsed globule or particle.
After cross-linking, the various SCNPs were exposed to dithiothreitol (DTT) to reduce the disulfide bond, thereby expanding the collapsed particles back into a solvated globule.
The anhydride based polymer was then exposed to different stoichiometric amounts of diamine (4-aminophenyl disulfide) cross-linker in order to see how compact the coils could be collapsed. Interestingly, it seems that 30% cross-linking is the limiting amount of cross-linker. This is most likely due to the fact that the polymer has become too compact to access the remaining internal anhydride moieties.
At this point catalytic amounts of FeCl3 was used as an oxidizing reagent to re-cross-link polymers back into SCNPs
The SEC plots in figure 3 demonstrates a full cycle of cross-linking, uncross-linking, and finally recross-linking again.
A representative sample of SCNPs was analyzed via TEM which agreed with the hydrodynamic radius value reported by viscometry.
Upon recross-linking, MALS showed the beginnings of self-assembled, reversibly cross-linked SCNPs.
Representative 1H NMR and FT-IR spectra showing the successful incorporation of the external, reversible cross-linker.
References:
O. Altintas, E. Lejeune, P. Gerstel and C. Barner-Kowollik, Polym. Chem., 2012, 3, 640.
T. Mes, R. van der Weegen, A. R. A. Palmans and E. W. Meijer, Angew. Chem., 2011, 123, 5191–5195.
E. J. Foster, E. B. Berda and E. W. Meijer, J. Polym. Sci., Part A: Polym. Chem., 2011, 49, 118–126.
E. B. Berda, E. J. Foster and E. W. Meijer, Macromolecules, 2010, 43,1430–1437.
E. Harth, B. V. Horn, V. Y. Lee, D. S. Germack, C. P. Gonzales,R. D. Miller and C. J. Hawker, J. Am. Chem. Soc., 2002, 124,8653–8660.
O. Altintas and C. Barner-Kowollik, Macromol. Rapid Commun.,2012, 33, 958–971.
J.-H. Ryu, S. Jiwpanich, R. Chacko, S. Bickerton and S. Thayumanavan, J. Am. Chem. Soc., 2010, 132, 8246–8247.
Bryan T. Tuten, Danming Chao, Christopher K. Lyon, Erik B. Berda