## Slide 1
S (LLV, 150 eV) and C (KLL, 265 eV) Auger peaks scale with varied TTPO coverage
C peak loses significance in prolonged study as it is present following thermal annealing beyond TTPO decomposition temperature ( T > 390º C) due to natural occurrence of carbon in UHV environment
S (LLV) is an excellent indicator peak of TTPO coverage as sulfur is unlikely to originate from other sources
Slow decrease of indicator peaks following thermal anneal, 250º C < T < 330º C, suggests desorption of molecules in surface layers above immediate substrate interface
Disappearance of S peak at T = 350º C likely indicates complete desorption of remaining TTPO monolayer
Thermal annealing for optimal TTPO SAM assembly safe for T < 300º C, but lower temperatures preferable
Additional TTPO (beyond monolayer coverage) may be removed through thermal annealing
The Auger Effect
Inner-shell vacancy is created by el high-energy (3-5 keV) electrons
Higher-shell electron transitions to fill vacancy (core hole)
Emission of Auger electron with energy, Eauger, characteristic of electronic structure.
Auger transition defined by participating electron orbitals (e.g., KLL)
Investigation of Trithiapentaceneone on Au(788) by Auger Electron Spectroscopy
Jeremiah van Baren1, Amanda Larson1, Jun Wang1, Jeremy Kintigh2, Glen P. Miller2, and Karsten Pohl1
1Department of Physics, 2Department of Chemistry University of New Hampshire;
NSF Center for High-rate Nanomanufacturing
Nanoscale Science and Engineering
Center for High-rate Nanomanufacturing
EEC-0832785
Abstract
Auger Electron Spectroscopy
TTPO Auger Spectrum, Indicators
Auger electrons pass between outer and inner shell
Shell bias determines energy of electrons incident upon detector
Materials and Methods
Novel pentacene derivative (TTPO), synthesized at UNH, on Au(788) substrate
Instrumentation contained in ultra-high vacuum chamber (~10-10 mbar)
Deposition and AES analysis performed in situ
TTPO deposited by physical vapour deposition (PVD)
Primary surface analysis and TTPO coverage determination by scanning tunneling microscopy (STM)
5,6,7-trithiapentacene-13-one
UHV Chamber
Molecular Self-Assembly
Governed by molecule-molecule and molecule-substrate interactions
Allows efficient production of molecular-scale architectures
STM image of Au(788)
(b,c) STM images of 6,13-dichloropentacene (DCP) SAM 1
(d) DFT model of free- standing DCP SAM 1
Cylindrical Mirror Analyzer
Auger Spectra
Signal intensity is extremely low; output differentiated to maximize peak sensitivity.
Surface composition determined by observed intensity of characteristic Auger peaks
Quantitative analysis difficult due to complexity of interaction
Auger spectrum of gold (Au)
Auger spectrum; cumulative TTPO deposition
(green) S (LLV, 150 eV), (red) C (KLL, 265 eV)
  Self-assembly of organic molecules can facilitate the efficient production of highly-ordered architectures1 on the molecular scale which have a wide range of applications in new materials and electronics.
  Thorough investigation of such surface assemblies requires microscopic methods, which are time-consuming and highly dependent upon pristine operating conditions.
  Auger electron spectroscopy (AES) provides rapid, surface-sensitive chemical analysis that greatly increases the efficiency of surface studies, including those of molecular assemblies.
  5,6,7-trithiapentacene-13-one (TTPO), a novel pentacene derivative synthesized by UNH Miller Group, is examined on vicinal Au(788) by AES to compliment scanning tunneling microscopy study.
Primary TTPO constituents are candidates for Auger “fingerprint”
Carbon: common surface contaminant; high concentration
Sulfur: low natural presence; high relative Auger sensitivity
TTPO deposited in 30 minute increments by PVD
STM image suggests sub-monolayer coverage after deposition time, t = 30 min.
Carbon and sulfur Auger peaks scale with varied TTPO deposition
Auger spectrum; cumulative thermal annealing
(green) S (LLV, 150 eV), (red)C (KLL, 265 eV)
Conclusions
Temperature Dependent Desorption
Auger spectrum; cumulative TTPO deposition;
normalized to substrate, Au, spectrum (black)
cumulative depositions pictured as red, blue, and green, respectively
References
[1] Wang, J., Kaur, I., Diaconescu, B., Tang, J.M., Miller, G.P., and Pohl, K. ACS Nano 2011 5 (3), 1792-1797
[2] Thompson, B., Tyson, C. Auger Electron Spectroscopy. In Chemical Analysis, vol. 74.; Wiley, 1985; pp 19-53.
Adsorbed species will desorb at some critical temperature when energy exceeds surface bonding
Indicator peaks dramatically decrease at T = 340º C
Comparatively small peak change for T < 300º C
Auger spectrum; cumulative thermal annealing;
normalized to substrate, Au, spectrum (black)
(green) TTPO 90 min., (red) 330º C anneal, (blue) 350º C anneal
3 keV
STM image; TTPO (ellipsoids in chains)
on vicinal Au(788); sub-monolayer coverage indicated;
deposition time, t = 30 min.
Benzene Rings (Carbon)