## Slide 1
Food
Cosmetics
Pharmaceuticals
Carbonless Paper
Textiles
Living cells
g = 0.28, c = 1 , l = 0.02, Re/Ca = 0.53
Fabrication and Characterization of Human Serum Albumin (HSA) Microcapsules
Christopher Blais and Nivedita Gupta
Department of Chemical Engineering
Motivation
Relevant Parameters
Fabrication of HSA Capsule
Drop Deformation Studies: Experimental versus Numerical
Ca = 0.42, k = 1.32
Ca = 0.83, k = 1.30
Numerical simulations predict breakup at lower Ca
Interfacial tension may be underestimated
g = 0.28, c = 1, l = 0.02, Re/Ca= 0.53
Q
z = 0
dd
Study capsules in constraining geometries
Flow induced deformation of diseased cells can be used to diagnose diseases
Summary
HSA microcapsules successfully fabricated
Robust capsules for 25% HSA solution with 30 minute reaction time
Dilatation and aspiration experiments set up to characterize capsules
Further Research
Conduct deformation studies to determine critical Elasticity number at which capsule breaks
Analyze how it changes with constraining geometry
Acknowledgements
Robert Carroll (PhD 2014 UNH)
UNH Hamel Center for Undergraduate Research
Brian Zukas (PhD 2016 UNH)
HSA capsule strength affected by reaction time and solution concentration
Future Work: Capsule Deformation Studies
Drain Bulk and wash with IPA and DI Water
HSA Drop formation in T-Junction
Crosslinking Reaction in Terephthaloyl Chloride forms membrane
Store capsules in Isotonic Saline Solution
10 cSt Silicone oil
20% wt. HSA in DI water
Chart: Area Dilation (DA/A0)
| 2.2407043626474249E-2 | 2.1817169784896812E-2 | 1.4495403483514156E-2 | 1.5638588678857448E-2 | 1.0715432627355737E-2 | 1.3136112499820418E-2 | 1.0049375590236611E-2 | 1.1409973773479146E-2 | 2.1898856047643273E-2 | 1.6623163084053837E-2 | 1.3481683546466755E-2 | 1.0971518002791321E-2
T (N/m) | 0.0038833 | 0.0039967 | 0.0027894 | 0.0028109 | 0.0019223 | 0.001939 | 0.00098545 | 0.0010046 | 0.003961 | 0.0028032 | 0.0018295 | 0.00099381
Optimization of HSA Capsule Fabrication
Characterization of HSA Capsule
Longer reaction times and higher HSA concentrations yielded more robust capsules
10 min 20 min 30 min 60 min
10%
20%
30%
13.9 kPa
9.86 kPa
6.4 kPa
3% NaCl
Smaller volume change of capsules observed at lower saline solution concentrations
Parameters Studied
CHSA - HSA concentration (percent by weight)
    10% , 20%, 30%
trxn - Reaction time
    10 min, 20 min, 30 min
25% HSA capsules show a compressibility modulus (K) of 164.5 mN/m
NH2
Chart: Time (min)
| 10.222222222222221 | 30.522222222222222 | 61.477777777777781 | 119.56111111111112 | 1174.5833333333333
10% | 0.89095 | 1.1329 | 1.4385 | 1.6992 | 2.3116
5.5% | 0.90478 | 1.0316 | 1.2789 | 1.4373 | 1.5218 | 1.5867 | 1.6338 | 1.6803
3% | 0.77573 | 0.78958 | 0.80343 | 0.83162 | 0.81728 | 0.83162 | 0.93646 | 1.0316 | 1.0817 | 1.5653
    Dilatation Studies
    Aspiration Studies
10% NaCl
Capsules are too rigid to pass through current geometry without lysing. Larger channel geometry and lower required
3mL/min, 25% HSA Capsule in 5.5 w/v salt solution
Numerical Simulation of a Capsule
Experimental setup
t = 0s
t = 0.96s
t = 2.60s