## Slide 1
Hydraulic Cylinder
Hydraulic System
Ball Screw Motor
DAQ & C Computers
Roller Assembly
Carriage
Bed
Rollers
Grip
Limit Switch
Grip
CBT Specimen
Carriage
Rollers
Grip
Limit Switch
Grip
CBT Specimen
Machine Specifications | Value | Units
Cylinder speed | 33.5 | mm/s
Carriage speed | 66 | mm/s
Cylinder force (retraction) | 312 | kN
Specimen elongation | 400 | %
Continuous-Bending-under-Tension
Continuous-Bending-under-Tension Machine and Experimental Setup
Ordinary Tension
Ordinary Plastic Bending
Plastic Bending Under Tension
Experimental Results
Result and Post-Processing
Project Objective: To understand the fundamental mechanisms behind Continuous-Bending-Under-Tension to implement in innovative manufacturing processes.
The Automotive Industry continues to face challenges as fuel consumption regulations increase. One of the major causes of poor fuel consumption is the weight of the vehicles. Using traditional metals, we cannot decrease the amount of material used without compromising the safety of the vehicles. By using high strength metals, we can use less material without sacrificing safety.
Motivation and Theory
Continuous-Bending-Under-Tension (CBT) allows us to incrementally deform a specimen. This is achieved by only allowing deformation to occur at the rollers. This is due to the specimen being plastically bent, which decreases the required axial load needed to deform the specimen. This process is know as bending-under-tension.
Timothy J. Roemer - Mechanical Engineering Department
CBT System Diagram
Top View of Carriage
CBT Carriage: Rollers, Specimen, Grips, Limit Switch
CBT Machine Tension Test Validation:
x is the ultimate tension strength
CBT Machine Specification
CBT System: Hydraulics, Ball Screw, Computer
CBT Specimen: 1x, 2x, 3x Regions (Uniform)
CBT Curve Analysis
CBT Tests For Different Roller Depth (δ) Per Thickness (t)
Advisors: Brad Kinsey, Yannis Korkolis, Marko Knezevic
CBT and Tension Test Specimens
Initial Specimen Image
Analysis of First Specimen
Black & White Contrast Intensity Image
Ellipsoid Identification & Measurement Image
Sponsors/ Partners: Ford Motor Company, Alcoa, U.S. Steel, National Science Foundation
Special Thanks: Vojta Kubec, Sheldon Parent, Madhav Baral, Peter Ripley, Chris Dick, Nengxiu Deng, Steve Racca, Joseph Wilson
Major & Minor Engineering Strain Percent Distribution
Major & Minor Strain Percent
Matlab Circle Grid Measurement