## Slide 1
Conductive Cellulose Materials Coated in Silver Particles
Karen Richards, Mehdi Jorfi, Sandra C. Espinosa, Jens Natterodt, Christoph Weder and E. Johan Foster
Adolphe Merkle Institute, Fribourg, Switzerland
University of
New Hampshire
Motivation and inspiration
Approach
Solving the ultra-high dilution problem
References
Acknowledgements
Cost projections
Indium tin oxide is a translucent and conduction material used as the conductive layer on liquid crystal displays (LCD), solar cells, smart phones.
Reasons for finding a replacement:
  Indium is a considered a ‘
  Price is steadily increasing
Proposed ITO replacement :
  Percolating network of silver supported
  on a network of cellulose nanocrystals
  Backfill with polymer
  Press into film
ITO (indium-tin oxide) | Coating Cellulose with Silver
Roughly $0.25-$0.69 to cover the LDC screen on an iPhone 5 | Roughly $0.02 to cover the LDC screen on an iPhone 5
Percolation model
“percolation on”
Mechanical properties of proposed material
Coating sulfonated tunicate cellulose aerogel with silver
Coating cellulose dispersion with silver
Sulfonated cellulose dispersion
Carboxylated cellulose dispersion
Two approaches
Kalowkamo J., Baker E. Estimating the manufacturing cost of purely organic solar cells. Elsevier. 2009. 83(8): 1224-1231.
Olsson R.T., Samir A.M.A.S., et.al. Making flexible magnetic aerogels and stiff magnetic nanopaper using cellulose nanofibrils as templates. Nature Nanotechnology. 2010.(5):584-588.
Hebb, H. Malcolm. Electrical Conductivity of Silver Sulfide. The Journal of Chemical Physics. 2004. 20 (1): 185.
Padalkar S., Capadona J.R., et. al. Natural Biopolymers: Novel Templates for the
Synthesis of Nanostructures. Langmuir Article. 2010. 26(11): 8497–8502.
Galland S., Anderson R.L., et. al. Cellulose nanofibers decorated with magnetic
nanoparticles – synthesis, structure and use in magnetized high toughness membranes for a prototype loudspeaker. Journal of Materials Chemistry C. 2013.13 (1): 7963-7972.
Schroers, M., Kokil, A. and Weder, C. (2004), Solid polymer electrolytes based on
nanocomposites of ethylene oxide–epichlorohydrin copolymers and cellulose whiskers. J. Appl. Polym. Sci., 93: 2883–2888o. di: 10.1002/app.20870
References
Acknowledgments
A special thanks to:
Adolphe Merkle Institute:
Christoph Weder, E. Johan Foster, Mehdi Jorfi, Sandra C. Espinosa, Jens Natterodt, Silvana Muller, Carola Endes, Janak Sapkota, Apiradee Nicharat, Sara Turner, and everyone at AMI.
University of New Hampshire:
Erik Berda and the Berda group for their continued support for the past four years.
Approach
Coating sulfonated tunicate cellulose aerogel with silver
Coating cellulose dispersion with silver
Sulfonated cellulose dispersion
Carboxylated cellulose dispersion
Multiple Potential Methods
All three methods above were tested to find the best for the desired application.
Tunicate cellulose aerogel
AgNO3
Reducing agent + surfactant + tunicate cellulose aerogel
Silver covered tunicate cellulose aerogel
Silver covered tunicate cellulose film
+
The method above describes the process of coating a sulfonated tunicate aerogel with silver.
c-CNC dispersion coated
in Silver particle
AgNO3
Water, CTAB (surfactant), NaBH4
The method above describes the process of coating a carboxylated/ sulfonated cellulose dispersion with silver. All materials were analyzed via scanning electron microscopy(SEM), and transmission electron microscopy (TEM).
Sulfonated CNC vs. carboxylated CNC
Function of reducing agent and surfactant
Sulfonated/ carboxylated
c-CNC dispersion
Reducing agent + surfactant
NaHBH4 (Reducing agent)
CTAB (Surfactant)
Both sulfonated and carboxylated CNCs where tested and analyzed.
Binding with sulfonated CNC
Binding with carboxylated CNC
Reducing agent: Sodium borohydride reduces silver nitrate to create a silver particle in situ.
Both a reducing agent and surfactant were critical in this reaction.
Surfactant (CTAB) changes the characteristics of the surface of the silver particle. This forms an attraction between the particle and the alcohol groups of the cellulose fiber.
Results
Results continued
Conclusion
Sulfonated tunicate aerogel:
Carboxylated tunicate dispersion:
SEM images of tunicate cellulose aerogels coated in 1.0 M AgNO3: (a) coated in gold in preparation for the SEM so the interaction between the silver and the cellulose fibers is visible (b) picture of the silver coated aerogel (c) was not covered in gold so the silver coating could be easily identified
b.
a
c.
The picture above shows dispersions with varying concentrations of AgNO3. TEM images were inconclusive due to difficulty in differentiating the silver particles.
Sulfonated CNC dispersion
  The best method to create a percolating network of silver on CNC’s
  TEM images
Carboxylated CNC dispersion
  TEM images were inconclusive
Tunicate cellulose aerogel
  The aerogel did not have an even coating of silver
  Cause:
  light-weight porous aerogel floats in solution and is not fully immersed
    The pores caused solution to be trapped and did not circulate throughout the aerogel
Chart: pH change of 1 mg/ml cellulose dispersion due to varying amounts of AgNO3
| 10 M | 1.0 M | 0.5 M | 0.1 M
pH before addition | 9.58 | 9.58 | 9.58 | 9.58
pH after addition | 5.96 | 7.1 | 8.91 | 9.4
TEM image of sample 2A with 1.0 M AgNO3
and 1.0 mg/ml sulfonated CNC’s
Results, shown in the chart and image above, indicate a correlation between the amount of AgNO3 added to the dispersion with both the color and pH of that dispersion.
Future work
Find a polymer that is both conductive and translucent when condensed into film with dispersion
  Possible polymers: LiClO4-doped ethylene oxide-epichlorohydrin (EO-EPI)
Coat polymer with silver sulfonated CNC dispersion, condense material into thin film, and characterize material
Sulfonated tunicate dispersion:
Plot of supply risk versus importance to energy of metals currently employed in the USA. (DOE Critical Materials Strategy 2011)
Adolphe Merkle
Institute