## Slide 1
Acknowledgments
I would like to thank the Advanced Inorganic Lab Staff as well as the entire UNH Chemistry Department for funding.
Introduction
Electrochromic devices alter their color, level of absorbance and level of refraction in a continuous and cyclical manner when a potential is applied.1 These electrochromic materials are used in smart windows, anti-glare windows, electrochromic mirrors, etc. Electrochromic devices are constructed from three components, of which one is a layer of a chromogenic complex. This experiment attempted to bind the RTIL trihexyltetracecylphosponium chloride [P6,6,6,14]Cl to various EDTA bound 3d transition metal salts. Cyclic Voltammetry was then used to demonstrate the redox gap.2
Figure 1. Reaction schemes for the synthesis of [P6,6,6,14]M(EDTA)
Figure 2. ATR-FTiR for Metal EDTA Salts of Cobalt, Manganese, and Iron.
Conclusions
The Metal-EDTA Salts of Chromium, Cobalt, Iron, and Manganese were synthesized in 15.7%, 60.5%, 94.7%, and 84.2% yield respectively. [P6,6,6,14]Co(EDTA) was synthesized in 63.7% yield. Completion of future work would allow for meaningful comparison of electrochemical features of the chromogenic complexes.
Future Work
Both the the reaction involving the binding of the RTIL to the Cr-EDTA Salt and the Iron-EDTA Salt would be attempted. The product from the manganese reaction would be isolated. All products including that of the cobalt scheme would be characterized by CV, 1H NMR, 13C NMR, and a time lapse UV/Vis Spectroscopy during electrolysis.
Figure 4. Cyclic Voltammetry analysis of [P6,6,6,14]Co(EDTA), 50mV/s (versus Ag/AgCl). Inset shows cyclic voltammetry of [P6,6,6,14]Cl in H2O.3
Experimental and Results
Due to time and resource constraints the RTIL [P6,6,6,14]Cl was only bound to the Co-EDTA Salt and the Mn-EDTA Salt. The RTIL was dissolved in ethanol and the Metal-EDTA Salt was dissolved separately in deionized water. The solutions were combined and allowed to stir under nitrogen. The manganese complex was never extracted from solution, there appeared to be a faint pink immiscible liquid. The cobalt reaction mixture was dried on a Schlenk line. This resulted in a purple sludge. Work-up yielded a viscous light purple oil. Cyclic voltammetry was attended to using a standard three electrode set-up.2
IR: 3017.48, 2996.44 (OH-enol), 1592.64 (C=O, C=C-enol), 711.12-1438.88 (CH, CN, C-O)
Experimental and Results
In equal equivalence disodium ethylenediaminetetraacetato dihyride, 1M NaOH, and the various 3d metal chlorides were refluxed under nitrogen for 1 hour. The resulting Metal-EDTA salts were refrigerated for various periods of time spanning between 1 day to 1 week until precipitate formed. NaFe(EDTA) and NaMn(EDTA) precipitated readily out of solution. Addition of ethanol was used to encourage precipitation of NaCo(EDTA) and NaCr(EDTA). All products were dried. ATR-FTiR spectroscopy was used to characterize all but NaCr(EDTA).2
IR: 3478.92, 3369.65 (OH-enol), 15.99.62 (C=O, C=C-enol), 720.35-1440.04 (CH, CN, C-O)
IR: 3027.84-3477.97 (OH-enol), 1671.81 (C=O, C=C-enol), 692.79-1444.64 (CH, CN, C-O)
Chromogenic Liquids: Synthesis of [P6,6,6,14]M(EDTA) Complexes using Various 3d-transition Metals
James Chase, Luke Fulton, Dr. Roy Planalp
jwq342@wildcats.unh.edu; Parsons Hall, 23 Academic Way, Durham NH 03824
The cyclic voltammetry analysis shows the redox activity of [P6,6,6,14]Co(EDTA) to be intrinsically different than that of the the RTIL. This in conjunction with the expected color change2 characterizes the product of the cobalt reaction scheme as the expected product [P6,6,6,14]Co(EDTA).
References
1Nicholson, R. S.; Irving. Shain (1964-04-01). Analytical Chemistry 36 (4): 706–723
2Chem. Commun., 2011,47, 2300-2302 Communication
3J. Phys. Chem. Lett., 2013, 4 (11), pp 1834–1837, 2013 American Chemical Society
Figure 3: Synthesized Metal EDTA Salts
Figure 5. Depiction of future experiments