## Slide 1: The effect of carboxylic acid additives on the structure and corrosion resistance of alumina coatings
Background & Theory
Methods & Materials
Figure 2. SEM cross-section image of anodized aluminum with 100mg Mellitic acid additive. Coating thickness: 27.7 μm.
Coating properties
Corrosion results
conclusions
In the aerospace, appliances, and computer industries, hardcoat anodizing is used to increase corrosion and abrasion resistance, improve surface cosmetics, and provide electrical insulation. Alumina is resistant at neutral pH, but is extremely vulnerable in acidic and basic environments such as household consumption and cleaning mediums. Varying anodizing bath additives and sealing chemistries are ways to improve the corrosion resistance of the coatings.
Complexing organic compounds in the form of carboxylates were added to the sulfuric acid anodizing bath to improve the stability of the coating.
Hard-ion carboxylates readily form complexes with Al3+ to form insoluble metal soaps that are incorporated onto the surface of the anodic coating. Ideally, this thin film promotes protection of the metal, and even more so when coupled with a finishing seal.1 Lithium acetylacetonate seal was chosen due to its ability to induce formation of a dual salt with good chemical resistance at the surface (Fig. 4).
Abby Koczera
Chemical Engineering 2017, University of New Hampshire
Figure 3. Potential with respect to time of additives anodized at various concentrations, includes measured coating thickness values.
Additive | Mass (mg) | Seal Types | Corrosion Tests
Mellitic Acid | 10 | None Boiling Water Boiling Lithium Acetylacetonate | 0.5M KOH 1M Acetic Acid
 | 100 |  | 
Glutaric Acid | 10 |  | 
 | 30 |  | 
 | 100 |  | 
Lithium Citrate | 10 |  | 
Experimental matrix
Higher concentrations of carboxylic additives in the anodizing bath yield thicker coatings
Additives create protective films composed of insoluble metal soaps
Lithium acetylacetonate seal provides protection against corrosion, specifically for glutaric acid configurations
Mellitic acid anodized samples performed best in KOH corrosion tests when sealed with boiling water
Table 1. Consequential additive configurations, including concentration in the anodizing bath followed by three types of seals and corrosion tests.
Figure 4. Lithium acetylacetonate sealing mechanism and its reaction with alumina.
Figure 1. Schematic of the flow process and experimental set up.
Metal Soap Complex
Figure 6. Corrosion behavior in 0.5M KOH for samples sealed in (a) boiling water and
(b) boiling lithium acetylacetonate. Sample (left to right in each photo): no additives, 10mg glutaric acid and 10mg lithium citrate.
(b)
(a)
G: Glutaric Acid
L: Lithium Citrate
M: Mellitic Acid
Figure 5. 0.5M KOH corrosion completion times for samples of different seals. Lithium acetylacetonate seal proved better than the hot water seal for all samples except Mellitic acid.
Increasing coating thickness
26.3μm
27.7μm
33.1μm
25.1μm
23.2μm
Potential vs. Time
Acknowledgements
The author acknowledges the guidance and expertise of Professor Dale P. Barkey, as well as the support of the University of New Hampshire College of Engineering and Physical Sciences.
40 minutes; 3.5 A/dm2
Type III Anodizing @ 0oC
DI Rinse
Clean
DI Rinse
Seal
Corrosion Tests
SEM & EDS
Analysis
Deionized H2O
Lithium Acetylacetonate
100oC, 15 mins
0.5M KOH
1M Acetic Acid
1M KOH
1min
Mellitic Acid
pKa = 0.8
Glutaric Acid
pKa = 4.34
Lithium Citrate
pKa = 3.13
Working Electrode
2cm2
Total Area
Aluminum Rods
Ice
10% vol H2SO4
0 < pH < 1
Potential (V)
Time (s)
10mg Glutaric Acid
10mg Mellitic Acid
100mg Glutaric Acid
100mg Mellitic Acid
None
Additive
Seal
LiAcAc
Water
Time (min)
Sample
1 μm
Additives