## Slide 1
Heo C and Yoo J. "The control of neural cell-to-cell interactions through non-contact electrical field stimulation using graphene electrodes" Biomaterials (2011) 32, 19-27.
[2] Kobelt LJ, Wilkinson AE, McCormick AM, Willits RK and Leipzig ND. “Short duration electrical stimulation to enhance neurite outgrowth and maturation of adult neural stem progenitor cells”. Annals of Biomedical Engineering (2014) 42, 2164–76
Light-Triggered Differentiation of Human Neural Stem Cells to Neurons
Alison Deyett , Salimah Hussien, and Kyung Jae Jeong
Department of Chemical Engineering, University of New Hampshire , Durham, NH, USA
Abstract
Background
Summary
Reactive Oxygen Species (ROS)
References
Acknowledgement
Neural tissue engineering aims to regenerate irreversibly damaged neural systems (either peripheral or central nervous systems) by differentiation of neural stem cells into neurons on three dimensional scaffolds by providing various chemical and physical cues. One physical cue that has received much attention is electrical stimulation by an external electric potential on conducting substrates such as graphene. One potentially useful method of achieving electrical stimulation of neural stem cells is by free electron generation on the surface of titanium oxide (TiO2) nanoparticles by light irradiation. However, the band gap of TiO2 nanoparticles is in the UV range which can be harmful to cells and has many limitations in clinical applications. The goal of this research is to develop a novel method to achieve visible light-triggered differentiation of human neural stem cells (hNSCs) into neurons. We have discovered that TiO2 grown on polydopamine (PDA) coated substrates exhibits an absorption peak in the visible light range. The surface chemistry was confirmed by various surface characterization methods including XPS, SEM and FT-IR. Using this substrate, we investigated the effect of laminin on hNSC adhesion, surface free electron generation on TiO2 by visible light irradiation, and preferential differentiation of hNSCs into neurons. The results from this research open up a new possibility for implantable neural tissue engineering scaffolds that can be activated by light irradiation.
Objective
Important for the future treatments many neurological conditions: stroke, spinal cord injury, ALS, Alzheimer’s disease, etc
Future work
Neural stem cells can be differentiated into two distinct lineages: neurons, or glial cells
Inducing an electric field on the cells can cause them to differentiate toward neurons [1].
Unfortunately inducing electrical field can be cytotoxic [1]
A current method relies on the generation of free electrons on the surface of titanium dioxide (TiO2) by UV irradiation [2].
UV irradiation causes chromosomal damages to the cells and has short tissue penetration.
Visible light is not harmful to cells and can penetrate tissue for implantable devices
Cell Attachment
To generate surface that generates free electrons under visible light irradiation to induce differentiation of hNSC into neurons.
Further ROS measurement tests to determine the necessary length of irradiation to generate free electrons
Long term cell study with light irradiation to and determine percentage of cells that differentiate into neurons over glia cells
Long term study with mesenchymal stem cells to determine if these cells can be turned into neurons using this technique.
Benjamin Stewart , Department of Physical Chemistry
Gonghu Li, Department of Physical Chemistry
Shujie Hou, Department of Chemical Engineering
Nancy Cherim and John Wilderman, University Instrument Center
McNair Scholar Program
TiO2 nanoparticles can be grown on polydopamine coated surfaces using (NH4)2 TiF6
Adding dopamine to the TiO2 nanoparticles adjusts the absorbance peak on the TiO2 and generates free electrons on the surface under light irradiation
The addition of more nanoparticles and dopamine enhances cell adhesion to the surface and promotes cellular elongation
The 24 hr-TiO2 hr compared to the 1 hr-TiO2 appeared to enhance cell adhesion
The addition of dopamine to the samples also enhanced cell adhesion to the surface
X-ray Photoelectron Spectroscopy (XPS)
Oxygen
Carbon
The titanium peak increases with reaction time indicating that more titanium oxide has been deposited on the surface
The peak also shifts to a lower binding energy in the addition of dopamine.
Scanning Electron Microscopy (SEM)
TiO2 Deposition - 1hr
TiO2 Deposition - 4hr
TiO2 Deposition - 24hr
As the reaction time increased the particle density of TiO2 also increased.
Crystalline structures begin to form after 24 hours
Surface Characterization
Titanium
As TiO2 is deposited on the surface, carbon peak begins to lose some of its characteristic peaks. This is caused by the titanium using the C-O as a binding site.
The oxygen peak changes significantly as the surface is coated with titanium. The bottom peak is representative of what the oxygen peak looks like for polydopamine, while the 24 hour sample peak matches the peak for TiO2
Absorbance
Deposition of TiO2 on polydopamine substrate results in a peak in the visible light range (420~430nm) that corresponds to ~2.8eV.
The addition of dopamine slightly increases the peak.
Chart: UV-Vis Spectrometry
Methods
Chart: 
 | 1 | 0.86746 | 1.5379
Glass
Relative Reactive Oxygen Species
24 hr-TiO2
24-hr TiO2+Dopamine
ROS was measured to determine the amount of free electrons on the surface of the TiO2 nanoparticles
The dopamine coating showed to generate higher amounts of ROS than others samples.