## Slide 1
Synthesis of p-xylene diisocyanide and Subsequent Polymerization to Form Poly(2,4-pyrrole-alt-p-phenylene)
Joey Mancinelli, Justin Cole, Erik Berda
jpm2006@wildcats.unh.edu, Department of Chemistry, University of New Hampshire, Durham, NH
12/9/16
Introduction:
Polypyrrole is a unique conjugated organic polymer that has many applications, including use in organic solar cells, batteries, and chemical sensors1. There are many reported ways of making 2,5 substituted polypyrroles, however synthetic routes to achieve 2,4 substituted polypyrrole have not been reported in the literature. This experiment is a novel synthetic route to 2,4 substituted polypyrrole (Scheme 1). It utilizes an efficient two-step organic synthesis to synthesize p-xylene diisocyanide starting from p-xylene diiamine. The p-xylene diisocyanide monomer will then be polymerized to afford poly(2,4-pyrrole-alt-p-phenylene) (Figure 1).
Figure 1. Poly(2,4-pyrrole-alt-p-phenylene)
Experimental Design:
A two-step synthesis was used to synthesis the diisocyanide (3) monomer, starting with a reflux of p-xylene diamine (1) in ethyl formate to afford p-xylene diformamide2 (2). P-xylene diformamide (2) was then dehydrated at room temperature with triethylamine and phosphorus (V) oxychloride in dichloromethane. This afforded p-xylene diisocyanide2 (3), which was then purified by column chromatography to afford purified (3) as a yellow oil2.
A cycloaddition polymerization of product (3) with copper (I) oxide, phenanthraline (ligand), and diethynlbenzene (4) as the second monomer was used to afford poly(2,4-pyrrole-alt-p-phenylene) (5).
Future Work:
The two-step synthesis used to synthesize the diisocyanide monomer will continue to be used in the future to obtain purified product (3). Further, the polymerization step (Scheme 1) which was unsuccessful in this experiment, will be used again to polymerize p-xylene diisocyanide and afford poly(2,4-pyrrole-alt-p-phenylene). Steps of the synthesis could also be performed with different reagents. For example, many reagents exist that can formylate the diamine. Examples include formic acid or formaldehyde3. Also, a different copper (I) source or a different ligand could be used in the cycloaddition polymerization.
Conclusions:
Synthesis of both the intermediate product and final product in the diisocyanide monomer synthesis were conclusive by 1H NMR characterization. However, further experimentation is needed to synthesize the final polypyrrole, as 1H NMR data shows no broadening of the peaks between the monomer NMR and the NMR taken of the polymer after the reaction ran for 24 hours.
Acknowledgements:
I would like to thank Justin Cole, Erik Berda, and the rest of Berda Research Group. I would also like to thank the University of New Hampshire Chemistry Department.
References:
Lange, U.; Roznyatovskaya, N. V.; Mirsky, V. M. Conducting polymers in chemical sensors and arrays. Analytica Chimica Acta 2008, 614, 1-26.
Daniel G. Rivera, DGR.; and Ludger A. Wessjohann, LAW. J. Am. Chem. Soc. 2006, 128, 7122-7123.
Gerack, C. J.; and McElwee-White, L.; Formylation of Amines. Molecules 2014, 19, 7689-7713.
Scheme 1. Synthetic route to obtain p-xylene diisocyanide and subsequent polymerization to obtain poly(2,4-pyrrole-alt-p-phenylene)2.
Results and Discussion:
Successful synthesis of both (2) and (3) are all conclusive based on NMR analysis, however the yields on both (2) and (3) were considerably low. Each product is characterized by NMR below and based on the spectrum synthesis of the (2) and (3) was successful. However, based on the NMR data for the polymerization of product (3), results do not show conclusively that polymerization was achieved to afford product (5), as there is an absence of broadening on the NMR of the polymer compared to the NMR of the monomer.
b
a
b
a
d
c
Figure 2. 1H NMR of diformamide, diisocyanide, and polypyrrole.