## Slide 1
Synthesis of 9,10 - Diphenylanthracene
Tom Williams, Arthur Greenberg, William Butler
tjw2001@wildcats.unh.edu, Department of Chemistry, University of New Hampshire, Durham, NH
December 9th, 2016
9,10 – Diphenylanthracene is a blue chemiluminescent dye that can be used in LED and non-electronic (fluorescent) lights.2 A bromination reaction and a Suzuki coupling reaction are utilized in the synthesis of the product; synthesis methods that are fairly simple and effective. 9, 10 -diphenylanthracene is a relatively expensive material and so a goal of the experiment is to efficiently synthesize it in the laboratory. If an efficient enough process is found it could become a considerably more affordable product and thus, more accessible in industry and research.
9, 10 – Diphenylanthracene was synthesized via a multistep synthesis using anthracene, with purity as a goal. The intermediate 9, 10 – dibromoanthracene was created through a bromination reaction in chloroform (Scheme 1).1 Once the intermediate had been formed, a Suzuki coupling was performed using phenylboronic acid over a tetrakis(triphenylphosphine)palladium(0) catalyst to form the title compound (Scheme 2).3
As a chemiluminescent molecule, 9,10 – diphenylanthracene emits light in the present of stimulants. Research at North Carolina State University indicates that the compound emits blue light in the presence of 1,2 – dioxetanedione, which would be the next logical step to this procedure, a process that is shown in Scheme 3. According to H1NMR spectra, one can claim that the products were pure; so further purification is not necessary.4
9,10 – Dibromoanthracene is easily synthesized using the bromination technique presented. The diphenyl product is slightly more difficult to create and requires an expensive catalyst. Through cost analysis (on Sigma-Aldrich) it was determined that the process used to create the product costed $140.47 per gram of product while analytical standard 9, 10 – diphenylanthracene costs $190.80 per gram, which interestingly shows the process used is more finically beneficial, however overhead and labor costs are not considered.
I would like to thank Professors Joiner and Greenberg and the UNH Department of Chemistry.
Chien, Wei-Lun., Yang, Chih-Min., Chen, Tai-Lin., Li, Shu-Ting., Hong, Jin-Long. Enhanced emission of a pyridine-based luminogen by hydrogen-bonding to organic and polymeric phenols. RSC Advances, 3, 6930-6938, 2013.
Serevicius, Tomas., Komskis, Regimantas., Adomenas, Povilas., Adomeniene, Ona., Jankauskas, Vygintas., Gruodis, Alytis., Kazlauskas, Karolis., Jursenas, Saulius. Non-symmetric 9,10-diphenylanthracene-based deep-blue emitters with enhanced charge transport properties. Royal Society of Chemistry, 16, 7089, 2014.
Suda, Mitsuru., Kai, Takahiro., Yamamoto, Toshihiro. Organic electroluminescent device having triptycene derivative material. US8906521 B2, December 9, 2014.
Wilson, Elizabeth. What’s that Stuff? Chemical and Engineering News. 77 (3), 65, 1999.
The bromination of anthracene was a very successful and simple reaction with excellent yield (75.2%). As 9,10 – dibromoanthracene is a very symmetrical molecule with only aromatic protons, two quartet peaks appear in the H1NMR spectrum due to long-range coupling, as indicated in Figure 1 below. The melting point also correlated perfectly with literature values, with the experimental range at 224.4°C – 225.3°C and the literature value from 223°C – 224°C. These factors together indicate great purity of the intermediate product.
The Suzuki coupling of 9, 10 – dibromoanthracene and phenylboronic acid yielded the desired product at 11.2%. The five specific peaks analyzed all appropriately appeared in the aromatic region of the spectra (Figure 2). With a melting point range of 242.5°C – 247.3°C some impurities were implied as theoretical melting point is 248°C - 250°C, however these are relatively unobservable on the H1NMR and so it was determined that product was pure, according to H1NMR spectra.
Future Work:
Conclusions:
Acknowledgements:
References:
Results and Discussion:
Introduction:
Experimental Design:
Scheme 1: Bromination of Anthracene
Figure 1: H1NMR of 9, 10 – Dibromoanthracene
Scheme 3: Chemiluminescenes of 9, 10 - Diphenylanthracene
Figure 2: H1NMR of 9, 10 – Diphenylanthracene
Scheme 2: Suzuki Coupling of 9, 10 – Dibromoantracene with Phenylboronic Acid
11.2% Yield
75.2% Yield