## Slide 1
Exploring the Synthesis and Internal Cross-Linking Abilities of Single Polymer Chains via Diels-Alder Reactions
Acknowledgments
I would like to thank Prof. Erik Berda and Ashley Hanlon for their help and enormous amount of support. I would also like to thank the UNH Department of Chemistry for their funding.
Jennifer Chouinard, Prof. Erik Berda
jmr386@wildcats.unh.edu; Parsons Hall, 23 Academic Way, Durham NH 03824
Introduction
Polymer synthesis is studied to gain an understanding of polymer units found in nature; proteins. Proteins are found in quaternary structures which can be broken down into tertiary structures and then into secondary structures, which include α-helices and β-sheets. These secondary structures are composed of primary structures which are perfectly sequenced polymers of approximately 20 possible monomers. The goal of my research was to synthesize linear random co-polymers using the monomers methyl methacrylate (MMA), furfuryl methacrylate (FMA), and a maleimide functionalized methacrylate (MIMA). I was able to explore the internal cross-linking abilities through thermal Diels-Alder (DA) chemistry between the pendant furan of FMA and the maleimide group of MIMA to form single-chain nanoparticles (SCNP).
References
Hanlon, A.M.; Martin, I.; Bright, E. R.; Chouinard, J.; Rodriguez, K. J.; Pantenotte, G. E.; Berda, E. B. Polym. Chem., 2017, Advance Article.
Zhang, Z.; Wang, W.; Xia, H.; Zhu, J.; Zhang, W.; Zhu, X. Macromolecules 2009, 42 (19), 7360-7366.
(3) Nguyen, N. H.; Levere, M. E.; Percec, V. Journal of Polymer Science Part A: Polymer Chemistry 2012, 50, 860-873.
(4) Konkolewicz, D.; Wang, Y.; Krys, P.; Zhong, M.; Isse, A. A.; Gennaro, A.; Matyjaszewski, K. Polymer Chemistry 2014, 5, 4396-4417.
(5) Pramanik, N. B.; Nando, G. B.; Singha, N. K. Polymer 2015.
Experimental
In a simple two-step synthesis using reagents 1-4, MIMA 5 was made. FMA 6, MMA 7, and MIMA 5 were polymerized using a copper-mediated controlled radical polymerization (CRP) technique. Monomer conversion was monitored using 1H NMR. The solution was worked up, precipitated in MeOH and collected as a white powder 82. 8 was diluted in DMF and heated to 120 °C overnight then cooled to room temperature, precipitated in MeOH and SCNP 9 was collected.
Conclusions
We developed a way to form SCNPs using simple thermal DA chemistry. Our synthetic design was easy and tunable throughout multiple approaches, such as RAFT and copper-mediated CRP. SCNPs utilize chemistry in a way to intramolecularly cross-link polymer chains, however, many approaches are not as easily modified. A one-pot internal folding to form SCNP was achieved using the random terpolymer of MMA, FMA, and MIMA and heating under dilute conditions.
Future Work
The work done after my experiments was to determine the reversibility of the internal cross-links using retro-DA chemistry. A series of experiments were performed to evaluate the strength of these DA adducts as cross-linkers, as this reaction is known in many cases to be reversible. Although, it has been reported that some elastomers incorporated with DA linkages show the formation of nonreversible DA adducts. With this system, it was verified that the DA adduct cross-links were essentially nonreversible5.
Results
Figure 1. Linear polymer chains internally cross-link to form SCNP1
Internal cross-linking
via thermal Diels-Alder chemistry
P1
MMA: 61.5%
FMA: 22.2%
MIMA: 16.3%
P2
MMA: 81.7%
FMA: 11.4%
MIMA: 6.9%
δ 3.5ppm: 1.00
δ 6.5ppm: 0.18
δ 7.4ppm: 0.12
δ 3.5ppm: 1.00
δ 6.5ppm: 0.06
δ 7.4ppm: 0.05
Discussion
MMA and FMA monomers were commercially available and the MIMA monomer was obtained through a simple two-step synthesis. The initial approach to polymer synthesis was through reversible-addition fragmentation chain transfer (RAFT) but was unsuccessful. Using a copper-mediated CRP technique, polymers were obtained as white powders. 1H NMR was used to determine the percent monomer incorporations3,4. Removal of the protecting group from the maleimide allowed for DA reactions to occur between the maleimide and furan pendant groups. SCNP formed easily by heating precursor polymers under dilute conditions
(1 mg/mL). MALS-SEC traces and 1H NMR spectra each indicated the formation of SCNP.
diene
dienophile
Sample | Mn [kDa] | Mw [kDa] | PDI | %FMA | %MIMA | Peak Retention Time (min)
P1 | 15.8 | 21.5 | 1.36 | 22.2 | 16.3 | 13.4
NP1 | 12.3 | 15.5 | 1.26 | - | - | 13.6
P2 | 9.4 | 12.5 | 1.33 | 11.4 | 6.9 | 13.5
NP2 | 8.7 | 10.3 | 1.18 | - | - | 13.5
Scheme 2. Polymer synthesis via copper mediated-CRP
Scheme 1. Synthesis of MIMA monomer
Scheme 3. Formation of SCNP
1
2
3
4
5
5
6
7
8
8
9
Figure 3. 1H NMR of P1 in CDCl3
Figure 2. 1H NMR of MIMA in CDCl3
Figure 5. 1H NMR of P2 in CDCl3
Figure 7. 1H NMR of NP1 in CDCl3
Figure 4. MALS-SEC trace overlays from parent polymer (P1) to nanoparticle (NP1)1
Figure 6. MALS-SEC trace overlays from parent polymer (P2) to nanoparticle (NP2)1
Figure 9. Mn, Mw, PDA, monomer conversions, and peak retention times2
Figure 8. Diels-Alder reaction mechanism between furan and maleimide pendant functional groups
2