## Slide 1
References
[1] F. Li, X. Duan, “Applications of layered double hydroxides”. Structure and Bonding 119 (2005).
[2] U. Costantino, F. Marmottini, M. Nocchetti, R. Vivani, “New synthetic routes to hydrotalcite-like compounds, characterization and properties of the obtained materials”. European Journal of Inorganic Chemistry 10 (1998) 1439-1446.
[3] A. Alvarez, R. Trujillano, V. Rives, “Differently aged gallium-containing layered double hydroxides”. Applied Clay Science 80-81 (2013) 326-333.
[4] B.P. Callahan, Y. Yuan, R. Wolfenden, "The Burden Borne of Urease“. Journal of the American Chemical Society 127 (2005) 10828-10829.
Introduction
Methods
Instruments
Thermogravimetric Analyzer (TGA)
The thermogravimetric analyzer (TGA) measures the mass of a sample in a defined atmosphere as it is submitted to a selected temperature program.
Applications
TGA could be used to gain understanding of any process with an accompanying change in mass, including:
Phase changes
Study of polymers
Dehydration
Catalysis-calcination/adsorption
Two different procedures were used to synthetize the Nickel-Gallium Layered Double Hydroxides:
Hydrothermal Method[2]
Urea Decomposition Method[3]
Two different calcination conditions:
500 ᵒC in 30%H2/He
500 ᵒC in ambient air
Hydrothermal
The hydrothermal method involves:
slowly mixing of nickel nitrate (Ni(NO3)2) and
gallium nitrate (Ga(NO3)3)
sodium carbonate (Na2CO3) and sodium hydroxide (NaOH)
125 ᵒC, 24 hr in a hydrothermal autoclave
Urea Decomposition
The Urea decomposition method involves:
using urea (CH4N2O) to precipitate the nickel
and gallium nitrates
continuous stirring in a silica oil bath
90 ᵒC, 24 hr
Thermogravimetric Analysis (TGA)
Hydrogen-Temperature Programmed Reaction (H2-TPR)
Conclusions
Micrometrics AutoChem II 2920
Micrometrics AutoChem II 2920 performs temperature programmed reactions by flowing a specified gas flow through a sample. The composition of the gaseous mixture is measured at the exit of the sample container with appropriate detectors.
Applications
Micrometrics could be used to gain information about:
Gas-catalyst interaction
Light-off temperature
Catalyst structure
Surface area
Layered Double Hydroxides (LDHs)[1]
LDHs are a class of ionic solids that could be used as catalysts for different applications
LDHs are characterized by a layered structure
Each layer is composed by combinations of two or three metal cations
The spacing between each layer is filled with anions and hydroxides groups
This Project
The chosen metal cations were Ni2+ and Ga3+
Two different synthetic approaches
Nickel/Gallium molar ratio = 3
Goals
Understand the structure and surface properties
Optimize parameters for each synthetic method
Characterize the LDH catalyst
Possible application for Ni-GA LDHs:
Carbon Dioxide Reforming of Methane to form Syngas
Future Work
Optimize Ni/Ga molar ratio
Characterizations including Fourier Transform Infrared Spectroscopy (FTIR)
Catalytic performance for Carbon Dioxide Reforming of Methane
Mettler Toledo TGA with STARe System
Micrometrics AutoChem II 2920.
a) Instrument and b) Gas flow chart
Typical single stage decomposition thermogravimetric curve
Urea decomposition mechanism in water[4]
Kiln Paragon Xpress Model E12T
Figure 2. Nickel-Gallium LDH prepared by Hydrothermal method. a) Thermogravimetric (TG) Curve and b) Differential Thermal Analysis (DTA) Curve.
Figure 3. Nickel-Gallium LDH prepared by Urea Decomposition method. a) Thermogravimetric (TG) Curve and b) Differential Thermal Analysis (DTA) Curve.
Figure 4. Hydrogen-Temperature Programmed Reduction (H2-TPR) profiles of Nickel-Gallium LDHS prepared by Hydrothermal Method and calcined at a) Air, 500 ᵒC and b) 30%H2/He, 500ᵒC.
Figure 5. Hydrogen-Temperature Programmed Reduction (H2-TPR) profiles of Nickel-Gallium LDHS prepared by Urea Decomposition Method and calcined at a) Air, 500 ᵒC and b) 30%H2/He, 500ᵒC.
Test Conditions:
heating rate of 5 ᵒC/min from room temperature to 650 ᵒC
pure nitrogen flow of 30 mL/minute
Test Conditions:
pretreat samples with pure helium at 150 °C, 30 min
heating rate of 5 ᵒC/min from room temperature to 450 ᵒC
10%H2/Ar flow of 30 mL/minute
Results
Figure 1. Thermogravimetric (TG) curve of Gallium Nitrate Hydrate (Ga(NO3)3•x H20).
The number of moles of water in the gallium nitrate hydrate was determined to be 6.
Chart: Temperature (ᵒC)
a)
b)
a)
b)
a)
b)
a)
b)
The sample prepared by Urea Decomposition Method contains a large amount of water
Calcination in 30%H2/He did not contribute to the formation of oxides
Enhanced reduction peak intensity for samples prepared by Hydrothermal Method
Reduction peak around 400 ᵒC is attributed to the reduction of Nickel (II) Oxide (NiO)
Ni-Ga LDHs synthetized by Hydrothermal Method and calcined in air show potential applications in catalytic reactions
Nickel-Gallium Layered Double Hydroxides: Synthesis and Characterization
Lorenzo Milani and Dr. Nan Yi Department of Chemical Engineering, University of New Hampshire
Acknowledgement
Special Thanks to:
  The Hamel Center for Undergraduate Research
  Department of Chemical Engineering
  Guoqiang Cao, Ph.D Student, University of New Hampshire
a)
b)