## Slide 1
Injectable Microporous Gelatin Hydrogel for Wound Healing and Tissue Engineering
and Innate Immune System and Tissue Integration of Microporous Scaffolds
Shujie Hou, Shiwha Park, Rachel Lake and Kyung Jae Jeong*
Department Chemical Engineering, University of New Hampshire, Durham NH, USA
I. Injectable Microporous Hydrogel
Acknowledgement
Research reported in this poster was partially supported by an Institutional Development Award (IDeA) from the National Institute of General Medical Sciences of the National Institutes of Health under grant number P20GM113131.
Despite many excellent properties of hydrogels for medical applications, poor bioactivity and lack of microporous structures often limit their applications in medicine. Here, we present an injectable porous hydrogel which has potential applications in facilitating the wound healing process. This novel formulation is composed of microgels made of gelatin, and these microgels are enzymatically crosslinked to form a bulk hydrogel with micropores created by interstitial space among microgels.
The average diameter of the gelatin microgels was 253 ± 155 µm, which results in interstitial spaces large enough for cells to grow in. The microgels formed a bulk hydrogel within minutes when mixed with mTG confirmed by rheology. The elastic shear modulus was comparable to that of nonporous gelatin hydrogel. The SEM image confirmed the three dimensional network of the bulk microporous hydrogel created by the interconnected microgels. Human dermal fibroblasts (hDFs) adhered and proliferated on the unmodified gelatin microporous hydrogel. This presents a significant advantage of using gelatin microgels over other widely used hydrogel systems on which cell adhesion and proliferation is minimal unless chemical modifications are made. The cellular infiltration was confirmed by confocal microscopy. The microporous gelatin hydrogel was also capable of releasing FITC-BSA at a controlled rate over two weeks.
This simple and cost-effective injectable porous microgel system is expected to find applications in wound healing and tissue engineering.
The gelatin microgels are co-injected with mTG to form a covalently crosslinked microporous hydrogel. This porous hydrogel serves as a temporary scaffold for cell infiltration and as a depot for therapeutic proteins for wound healing.
Optical Microscope
500 µm
FITC-BSA Loaded Microgels
Controlled Release of FITC-BSA
Confocal Microscopy
Hydrogel formed by microgels
Non-porous bulk hydrogel
Cell proliferation
Hydrogel formed by microgels
Non-porous bulk hydrogel
Cellular infiltration into the interstitial space
Rheology
Scanning electron microscopy (SEM)
*
*
II. Innate Immune System and Tissue Integration
Tissue growth into the pores 45 days after subcutaneous implantation
Tissue integration of microporous scaffolds measured by mechanical pulling test
Rupture force vs foreign body giant cells (FBGCs)
Research is underway to find correlation between macrophage polarization and tissue integration of tissue engineering scaffolds.
This research will help us find optimal scaffold design for tissue engineering.
Host integration of tissue engineering scaffolds is essential for the full regeneration of the damaged tissue.
Innate immune system, more specifically macrophages, are known to be the major determinant of host integration of the implanted materials.