## Slide 1: Troubleshooting the Electrochemical analysis of elastin-like polymers Alexis F. Mack,a Marissa Morales,b Eva Rose M. Balog,c and Jeffrey M. Halpernb aDepartment of Molecular, Cellular, and Biological Sciences, University of New Hampshire bDepartment of Chemical Engineering, University of New Hampshire cDepartment of Chemistry and Physics, University of New England
.
Elastin-Like Polymers (ELP) are stimuli-responsive smart polymers
  Consist of a 25 amino acid penta-peptide repeat, VPGIG
  Not electrochemically active
  Two constructs
        K-ELP contains 3 lysine residues
        C-ELP contains a cysteine residue prior to repeats
  Thiol Attachment Method leads to Covalent linkage between cysteine residue of C-ELP and Au surface
  TCEP- reducing agent used to prevent disulfide bridge formation
    Performed at 4°C to ensure C-ELP is in its elongated, monomeric form
Amide Chemistry
Requires 11-mercaptoundecanoic acid to activate surface with carboxyl groups
Amide linkage between lysine residue on K-ELP and the carboxyl groups
Introduction
  Ferrocene is a widely used electrochemical tag
    However, highly insoluble in H2O
  Ferrocene-NHS ester- expected to covalently bond with the NH3+ on K-ELP
    Ferrocene-NHS ester 10x excess to bind all NH3+
    Excess ferrocene-NHS ester removed via desalting
  Expected Mechanism:
Inability to solubilize conjugated ferrocene-NHS ester-K-ELP
  Inability to desalt conjugation because protein remained in desalting column
Inconclusive results on extent of conjugation due to solubility issues
  Addressed this by modifying a sensor for other electrochemical analyses
Sparse monolayer coverage of C-ELP
May be due to experiment duration
  Insufficient –SH contact with Au
Bio-conjugation
Revisit potential electrochemical tags
  Must be soluble in H2O
  Undergo a characteristic transition based on the external environment
    pH, temperature, and ion concentration responsive
    Transition has yet to be monitored electrochemically
      Requires production of an electrochemically active polymer
      Or
      Use Electrochemical Impedance Spectroscopy (EIS)
        Eliminates need for producing an electrochemically active ELP
Bio-Conjugation Method
Thiol Attachment Method
EIS Method
Bio-Conjugation Results
Bio-Conjugation Discussion
Fig. 1. Gel electrophoresis results of the control bio-conjugation groups
Fig. 2. Gel electrophoresis results of the experimental bio-conjugation groups
Thiol Attachment Results
EIS Results
Fig. 3. AFM analysis of a bare Au-coated quartz crystal
Fig. 4. AFM analysis of a C-ELP modified Au-coated quartz crystal
Thiol Attachment Discussion
EIS Discussion
Future Work
Acknowledgements
SEEDS Laboratory
NSF CBET 1638896
UNH Student Chapter ASBMB
UNH Hamel Center for Undergraduate Research
Ferri/ferrocyanide solution (Fe2+/Fe3+) allows for electron transfer
  Electron transfer measured via EIS
Used C-ELP modified Au-coated quartz as sensor
  Ran a heat profile (4°C - 40°C) and cooling profile (40°C - 4°C)
C-ELP collapse in response to heating expected
  Collapsed ELP will impede electron transfer at the sensor surface
https://www.omicsonline.org/JMBTimages/JMBT-S6-004-g002.html
Analyzed using a Randles Circuit and Nyquist Plot
Fig. 5. Heating profile on a bare Au-coated quartz crystal
Fig. 6. Heating Profile on a C-ELP modified Au-coated quartz crystal
Chart: Z real
Chart: Z real
Bare Au-coated quartz crystal RCT change = ~250 Ω between 25°C - 50°C
C-ELP modified quartz crystal RCT = ~550 Ω between 25°C - 50°C
Unsure of RCT change implications
  Lack of uniform C-ELP coverage
  Temperature increase may be influencing the RCT