## Slide 1
Low-Pressure Results
Air-Sensitivity and Degradation of Black Phosphorus
Cam Flynn, Ben St. Laurent, Jake Riffle, and Shawna Hollen
Department of Physics, University of New Hampshire, Durham, NH 03824
Introduction
Motivation
Two-dimensional (2D) crystalline materials have the potential for flexible components that remain highly conductive. Applications range from circuit components to energy generation. Black phosphorus (BP) is a semiconducting crystal recently isolated in a 2D sheet. It combines the higher on/off ratio of transition metal dichalcogenides with the high mobility of graphene, making it ideal for transistors[1]. It also is very robust against mechanical strain, so it is interesting for flexible electronics[2]. However, one drawback is its rapid oxidation in air, which degrades its electrical properties.
Using a low-temperature, ultra-high vacuum scanning tunneling microscope (STM) from RHK Technology and four-point probes by Capres, we were able to investigate the oxidation reaction of bulk BP and flakes.
References and Acknowledgements
X. Ling, et al. “The Renaissance of Black Phosphorus”. PNAS, 112 (15). 2015.
W. Zhu, et al. “Flexible Black Phosphorus Ambipolar Transistors, Circuits and AM Demodulator”. Nano Lett., 15 (3). 2015.
K. Utt, et al. “Intrinsic Defects, Fluctuations of the Local Shape, and the Photo-Oxidation of Black Phosphorus”. ACS Cent. Sci., 1 (6). 2015.
Y. Huang, J. Qiao, et al. “Interaction of Black Phosphorus with Oxygen and Water”. Chem. Mater., 28 (22). 2016.
Z. Hu, Q. Li, B. Lei, et al. “Water-Catalyzed Oxidation of Few-Layer Black Phosphorus in a Dark Environment”. Angew. Chem., 56 (31). 2017.
B. Kiraly, et al. “Probing Single Vacancies in Black Phosphorus at the Atomic Level”. Nano Lett., 17 (6). 2017.
J. Riffle, et al. “Impact of Vacancies on Electronic Properties of Black Phosphorus Probed by STM”. J. App. Phys. 123 (4). 2018.
We are glad to acknowledge that funding for this project was provided by the UNH Center for Advanced Manufacturing and Materials Innovations (CAMMI) Seed Grant Program and the Hamel Center for Undergraduate Research. I would like to thank my group members and collaborators for their help and cooperation with this project.
Fig. 1: BP has the combined properties of graphene and TMDs[1].
Fig. 2: The transistor characteristics of BP show no marked difference after 5000 bending cycles[2] .
Fig. 11: STM image of the pristine surface before exposure to adsorbates. Atomic rows are visible here. Dumbbell defects are phosphorus vacancies that are inherent to the sample[6,7].
Figure 3 shows that the theoretical activation energy for O2 molecule dissociation at a defected crystal site in BP is significantly less than it is at a pristine lattice site. The lower energy is closer to the optical range, so that light should help with the reaction [3].
To the right are the results of a study done to show the effects of water and light (Images a, b, and c) versus deaerated water and light (Images e and f) on black phosphorus[4]. Images a, b, and c are taken immediately, and then after one and two weeks in water, respectively. There is some clear degradation, especially noticeable in the thinner regions. Images e and f were taken in deaerated water, and there is no discernable difference, even in the thin layers.
Figure 5 [5] shows the effects of water and oxygen exposure versus water and nitrogen exposure in the dark by XPS. On the left there is a phosphoric oxide peak that starts to grow in time, signaling a shift in chemical makeup of the crystal. On the right, water and nitrogen does nothing to the crystal.
Before experiments, we image the surface to ensure it truly is pristine after cleaving, as shown to the right in figure 11. Dumbbell shapes are inherent structural defects studied extensively by us[6,7].
Figure 12 is the four-point resistance versus time graph for pure oxygen exposure. For the first 90 minutes the sample was in vacuum. Then we leaked pure oxygen into the chamber at 5x10-5 mbar, with some light. At hour 18, we shined a more intense (halogen) light on the sample, with the pure oxygen leak ongoing.
Figure 13 is the same as figure 12, but for atmospheric air exposure. Air was introduced immediately, again at 5x10-5 mbar. Light was introduced at hour 16.5 by halogen bulb.
In both cases, we clearly see there is no effect on the four-point resistance of the sample at these pressures and on these timescales. Future work should focus on finding the critical pressure for a significant change in resistance to occur in bulk samples as well as flakes.
1
2
4
5
3
Methods and Equipment for Controlled Exposure
To carry out this experiment, we controlled air exposure into the chamber while taking four-point measurements.
Image pristine surface of bulk BP
Take four-point measurements in vacuum without light exposure
Leak in gas at 5x10-5 mbar, continue four-point measurements without light exposure
Expose to light, continue four-point measurements
Image adsorbate-exposed BP surface
Air-free preparation is done in a nitrogen glovebox (Caputo group, UNH Chemistry). Samples are cleaved and mounted there and transported to the UHV system by a nitrogen-filled transit chamber.
The four-point probes made by Capres range in size from 5 to 30 microns between the outermost pins. Our UHV system allows us to control the probe landings on the nanometer scale with piezomotor controllers. We built an angle-adjustable probe stand for the probes to attach to.
5
References:
13
12
Fig. 10: Optical images of degradation of black phosphorus in air, over a two day timeframe
To the left (Figure 10) are a series of optical images of black phosphorus degrading in air over the timescale of two days. The discolored spots are oxidation patches, which grow over time.
We home-built a millimeter-scale probe, shown on the left in Figure 7 landed on bulk black phosphorus. Instead of the gold wires which attach to the cantilevers, as in the Capres design (on the right), we made macroscopic copper cantilevers that can be positioned by hand.
Our vacuum chamber operates at 10-10 mbar, with a temperature-controlled stage in the probe station (the left subchamber in Figure 9).
6
8
10
11
9
Capres Probes: www.capres.com
7
1 mm
1 cm
5 μm