## Slide 1
Steven Arias, Tan Dao, Shawna Hollen
Department of Physics, University of New Hampshire, Durham, NH 03824
Scanned probe microscopy studies of MoS2 catalysis on insulating substrates: investigating the impact of substrate, strain, and defects
Currently around 37% of the U.S. energy consumption is from petroleum.1 Environmental concerns are now prompting stricter government regulations and motivating ultra-deep sulfur removal from petroleum products.
Due to their performance and natural abundance, MoS2 and WS2 catalysts have been used on an industrial scale for hydrodesulfurization (HDS) of oil feedstock since World War II.2,3
Despite more than 50 years of industrial use, the fundamental mechanisms for the HDS reaction on MoS2 and the importance of the two-dimensional nature of the catalysts have only started to be understood in the last decade.
Ultra Low Sulfur Petroleum
We investigate the role of substrate, strain, and lattice defects on the HDS reaction in two novel experimental systems using non contact Atomic Force Microscopy (nc-AFM):
We would like to acknowledge the American Chemical Society Petroleum Research Fund for funding this project.
Collaborators: Todd Gross (UNH Mechanical Engineering), Young Jo Kim (UNH Electrical Chemical Engineering)
MoS2 flakes on SiO2/Si:
Flat.
Insulating.
Can be studied with nc-AFM.
Atomic Force Microscopy (AFM) extends scanning probe techniques to non-conductive materials.​
Beyond simply being an alternative to STM for insulating samples, it has been shown that AFM with a properly functionalized tip is capable of higher spatial resolution than STM, for example, revealing the molecular structure of pentacene5.​
MoS2 flakes on AAO
Raman Spectroscopy
Previous work done by the Besenbacher group at Aarhus University using Scanning Tunneling Microscopy (STM) revealed the role of the catalytically active MoS2 edges. All STM experiments on MoS2 catalysis have used metal substrates.4
MoS2 sheets on anodized aluminum oxide (AAO):
Holes and Undulations.
Adds Strain
Adds areas for suspension.
Can be studied with nc-AFM or STM.
The left image shows the Raman peaks for 4 different flakes. Red being the thickest and green the thinnest.
From [4]. (A) Thiophene on Au(111), (B) Line scan of the STM image. Red line is an edge with an adsorbed molecule. Black line is a clean edge. (C) Cut out from image A showing the structure of the adsorbed molecule.
From [5]. (A) Molecular model of pentacene. (B) STM scan.
(C-D) AFM images of pentacene, showing the molecular structure.
In the Hollen Lab, we use a non-contact AFM technique, with a qPlus6 probe, in which a tuning fork with a sharp tip is driven to oscillate in proximity to the surface we want to study. ​
Subtle changes to the oscillation frequency result from changes in the height of the surface, allowing us to map the height with high precision.​
qPlus AFM sensors
Nc-AFM images of MoS2 flakes on SiO2/Si
1.Image source: U.S Energy Information Administration
2. H. Topsøe, B. Clausen, and F. Massoth, “Hydrotreating Catalysis,” in Catalysis–Science and Technology, Vol. 11 (J. R. Anderson and M. Boudart, eds.), Berlin, Heidelberg: Springer Berlin Heidelberg, 1996.
3. A. Stanislaus, A. Maraﬁ, and M. S. Rana, “Recent advances in the science and technology of ultra low sulfur diesel (ULSD) production,” Catalysis Today, vol. 153, no. 1-2, pp. 1–68, 2010.
4. J. Lauritsen, M. Nyberg, R. Vang, M. Bollinger, B. Clausen, H. Topsøe, K. Jacobsen, E. Laegsgaard, J. Norskov, and F. Besenbacher, “Chemistry of one-dimensional metallic edge states in MoS2 nanoclusters,” Nanotechnology, vol. 14, no. 3, pp. 385–389, 2003.
5. L. Gross, F. Mohn, N. Moll, P. Liljeroth, G. Meyer. Science, 325, pp 1110--1114 (2009)
6. qPlus is a trademark of Professor Franz Gießibl
7. C. Rice, R. J. Young, R. Zan, U. Bangert, D. Wolverson, T. Georgiou, R. Jalil, K. S. Novoselov, “Raman-scatterin measurements and first principle calculations of strain-induced phonon shifts in monolayer MoS2,”Physical Review B 87, 081307(R), 2013.
8. C. Lee, H. Yan, L. E. Brus, T. F. Heinz, J. Hone, S. Ryu, “Anomalous lattice vibrations of single- and few-layer MoS2,” ACS Nano, 2010, 4(5), pp 2695-2700.
Substrate Dependent Catalysis
MoS2 Catalysis on Gold
Acknowledgements
qPlus Atomic Force Microscopy
Investigating Strain
References
The images to the left show the edge of a MoS2 flake on SiO2/Si. This edge is a promising area to observe the interactions between adsorbed thiophene molecules and MoS2.
Similarly we will image MoS2 on AAO to look for any changes.
These experiments will help us understand the role of MoS2 as a catalyst in hydrodesulfurization reactions used in industry
Atomic Force Microscopy images of a flake of MoS2 on top of the AAO substrate. The holes and undulation pattern on the AAO are visible even through thin layers of the MoS2
Under strain we would expect to see phonon shifts in few layers of MoS2 flakes using Raman.7
The non-resonant Raman spectrum of MoS2 is dominated by two vibrational modes: E12g and A1g. These two modes are sensitive to the number of layers a flake has. As the layers increase the peaks shift away from each other.8
E12g
A1g