## Slide 1
Investigation of the Sensing and Stability Characteristics of a Nickel (II) Oxide Film
Charlie Gasperoni, Christian Tooley, and Jeffrey M. Halpern
  Nickel was deposited on the electrode by sweeping the potential from -0.8V to 0V for 40 cycles in 2mM Ni(NO3)2
  The surface was then passivated by flowing 0.1 M NaOH and sweeping from 0V to 0.6V for 40 cycles
  Primary Method used was Cyclic Voltammetry, a potential sweep in a cyclic manner
  Current response is measured and translated into a Cyclic Voltammogram
  Oxidation and Reduction activity is commonly perceived as peaks and waves in the graph
  Polarization Resistance is a non-destructive technique that can be used to calculate corrosion data
  By shifting the voltage from its resting potential and recording the current change, one obtains a Polarization Resistance Curve
  The corrosion rate can be extrapolated by fitting a tangent line to the point where zero external current is flowing, and then using the equation below.
CR = Icorr * Kp * μeq / ρ * A
CR: Corrosion Rate Kp: Constant (Defines Units)
Icorr: Corrosion Current μeq: Equivalent Weight (Atomic Weight / # of electrons transferred)
ρ: Density of material A: Area of sample
Acknowledgements: Thanks to the Department of Chemical Engineering at the University of New Hampshire, The Hamel Center for Undergraduate Research, The SEEDS Lab, NIH P20 GM 113131
Chart: I (A)
Chart: I (A)
Chart: I (A)
Chart: I (A)
Corrosion Rate: 1.960 x 10-3 mpy
Corrosion Rate: 2.088 x 10-3 mpy
Corrosion Rate: 2.035 x 10-3 mpy
Corrosion Rate: 3.354 x 10-3 mpy
Chart: Potential / V vs. Ag/AgCl
Chart: Potential / V vs. Ag/AgCl
Chart: Potential / V vs. Ag/AgCl
Chart: Potential / V vs. Ag/AgCl
Chart: V vs Ref (V)
Chart: V vs Ref (V)
Sensing experiments were done using a glassy carbon electrode in a standard 3 electrode flow cell
Stability experiments utilized an amorphous carbon electrode in a 3 electrode eQCM setup
Ag/AgCl was used as the reference electrode
Platinum was used as the counter electrode
Chart: time
Chart: time
Chart: voltage
Sensing
Stability
0.1 M NaOH used as Blank Sample
Blank 0.1 M NaOH Corrosion Rate: 2.026 x 10-3 mpy
Conclusions
    No clear trend of current versus concentration
    Interested in investigating the surface stability
Conclusions
    Corrosion of the metal oxide film could be being accelerated by arginine
    A Schiff-Base Complex is formed between NiO and Arginine, increasing the solubility of the metal
Modification Technique
Experimental Setup
Background
  Nickel oxide surfaces have known electrocatalytic properties1
  Amino acids are common biomarkers of many diseases2
  The sensing capabilities of a Nickel (II) Oxide film was analyzed, as well as the electrochemical stability.
  Roushani, M., Shamsipur, M. & Pourmortazavi, S.M. (2012), J Appl Electrochem, 42: 1005.
  Woo, H. , Chun, M. , Yang, J. , Lim, S. , Kim, M. , Kim, S. , Myung, W. , Kim, D. and Lee, S. (2015), CNS Neurosci Ther, 21: 417-424.
Alanine
Serine
Arginine
Valine
Alanine
Serine
Arginine
Valine
Stability Method
Sensing Method