## Slide 1
RR
RR
Revealing the Role of Water in Hydrophobic Waterborne Polymers via Differential Scanning Calorimetry(DSC)
Chang Liu, Amit Tripathi and John Tsavalas
Department of Chemistry
University of New Hampshire, Durham, NH, USA
s
Acknowledgements
UNH Latex Morphology Industrial Consortium for its funding
Department of Chemistry in UNH.
Dr. Tripathi’s insightful discussion.
Prof. Tsavalas’s helpful advising.
Support from all our group members.
References
Conclusions
Result & Discussions
Figure 2: Theoretical non-freezable water content contribution of chemical structures and polymer chemical structures used in this research.
Figure 1: Typical DSC curve assignments. The top represents the peak assignments for different types of water, The bottom represent the polymer Tg peaks.
Objective
The developments of three different types of water in the hydrophobic waterborne polymer are qualitatively and quantitatively characterized via DSC.
Three effects on the distribution of three types of water in the polymer matrix are evaluated. These three effects are water content, surfactant concentration and polymer chemical composition.
The influence of water on the polymer property change is evaluated.
Hydrophobic waterborne polymers are synthesized as a dispersion in water and applied widely in coatings, adhesives and dental materials. Water can associate with it in three states: free water, freezable bonded water and non-freezable bonded water.
Glass Transition Temperature (Tg) Change
Hydroplasticizatio
Softer
n
n
n
n
n
n
n
n
Outside layer to inside layer:
Non-freezable water;
Freezable bonded water;
Free water.
Higher interaction
Lower interaction
Scheme 1: A Flow Chart for Experimental Approaches.
Major
Contributors
5e-5
0.005
0.1
0.2
0.3
1.3
2.0
11.3
Minor
Contributors
Structural
Group
#
Where # =
Moles H20
@ R.H. =1.0
Latex Polymer analyzed
MMA/MA
STY/BA
More Hydrophilic
More Hydrophobic
=
All chemical structures in the polymer can contribute to non-freezable water content in the polymer. The non-freezable water content can hydroplasticized the polymer and make its Tg drop down to wet Tg.
The wet Tg can be calculated based on the non-freezable water content in the polymer according to the wet Tg calculation equation. Here is a weight fraction of polymer and is a weight fraction of non-freezable water in the polymer. is the dry Tg of polymer, which can be obtained from DSC signal.
Equation 1: Wet Tg calculation based on Fox equation.
(-137 ℃ is used as a Tg for pure water)
Result & Discussions
Sample | Chemical Composition (wt%) | Theoretical Non-freezable water content (wt%) | Dry Tg (℃) | Theoretical wet Tg (℃)
MMA/MA | 71:29 | 3.76 | 75.5 | 56.16
STY/BA | 75:25 | 0.8 | 65.9 | 61.9
Table 1: General information for polymers used in this research.
Chart: W𝑓nw for MMA-MA samples with different water content added
| 1 | 3 | 5 | 7 | 9 | 11 | 13 | 15 | 17 | 19
24wt% water added | 0 | 0.034179 | 0.035587 | 0.034649 | 0.036289 | 0.036172 | 0.03699 | 0.037263 | 0.038351 | 0.037885
29wt% water added | 0 | 0.04054 | 0.041021 | 0.044635 | 0.043636 | 0.044592 | 0.045285 | 0.045155
33wt% water added | 0 | 0.023083 | 0.028025 | 0.030533 | 0.030842 | 0.030308 | 0.031376 | 0.035456 | 0.036151
10wt% water added | 0 | 0.022534 | 0.028122 | 0.031241 | 0.033045 | 0.033835 | 0.034276 | 0.034686 | 0.034812 | 0.035127
15wt% water added | 0 | 0.018947 | 0.024746 | 0.027735 | 0.030021 | 0.032107 | 0.033241 | 0.034524 | 0.0349 | 0.03614
Theoretical line (3.76wt%) | 0.0376 | 0.0376 | 0.0376 | 0.0376 | 0.0376 | 0.0376 | 0.0376 | 0.0376 | 0.0376 | 0.0376 | 0.0376 | 0.0376
Water added | Experimental wet Tg (℃) | Calculated wet Tg (℃)
24wt% | 56.17 | 55.81
29wt% | 56.32 | 52.54
33wt% | 55.73 | 57.22
10wt% | 56.09 | 57.53
15wt% | 55.9 | 56.88
Dry
DSC Analysis
Approach & Considerations
Chart: W𝑓nw for different polymer samples
| 1 | 3 | 5 | 7 | 9 | 11 | 13 | 15 | 17
STY-BA(hydrophobic) | 0 | 0.0060955 | 0.0097173 | 0.011406 | 0.01178 | 0.012267 | 0.012304 | 0.012229 | 0.012865
MMA-MA(hydrophilic) | 0 | 0.034179 | 0.035587 | 0.034649 | 0.036289 | 0.036172 | 0.03699 | 0.037263 | 0.038351
STY-BA theoretical | 0.008 | 0.008 | 0.008 | 0.008 | 0.008 | 0.008 | 0.008 | 0.008 | 0.008
MMA-MA theoretical | 0.0376 | 0.0376 | 0.0376 | 0.0376 | 0.0376 | 0.0376 | 0.0376 | 0.0376 | 0.0376
(1)
(2)
(3)
How to calculate non-freezable water content from the melting peak shown in DSC curve?
Assume no water adsorption happening in the first heating cycle.
Any decrease on the area under water melting peak can be attributed to the increase of non-freezable water content.
Here, and are the areas under water melting peak in the first heating cycle and the Nth heating cycles, respectively. represents the total water content added into the sample. is the mass of the whole sample, and is the mass of polymer added in the experiment.
Sample | Experimental wet Tg (℃) | Calculated wet Tg (℃)
STY-BA | 59.50 | 59.55
MMA-MA | 56.17 | 55.81
Figure 3: Experimental non-freezable water content for different polymer samples.
Figure 4: Experimental non-freezable water content for MMA-MA samples with different water content added.
Table 2:Comparisons between experimental wet Tg and calculated wet Tg for different polymers .
Table 3:Comparisons between experimental wet Tg and calculated wet Tg polymers different MMA-MA samples
Non-freezable water contents given by DSC results can match the theoretical number very well for both hydrophobic and hydrophilic samples.
The water content will not affect the final non-freezable water content, because the number of site for water-polymer bonding is limited by polymer chemical composition.
The experimental reproducibility is high.
Figure 5: The influence of surfactant (SDS) on non-freezable water content in the sample.
Ionic Sulfate Group.
Figure 6: The structure of the surfactant (SDS).
Polymer with SDS can have much higher W𝑓nw , because of the sulfate group in SDS.
Three types of water in polymer matrix can be qualitatively and quantitatively characterized via DSC.
The non-freezable water can change the polymer properties a lot.
Non-freezable water content will not be affected by water content added but can be significantly affected by the polar surfactant.
Tsavalas, J. G.; Sundberg, D. C. Langmuir 2010, 26 (10), 6960–6966.
Lei, Y.; Child, J. R.; Tsavalas, J. G. Colloid Polym. Sci. 2013, 291 (1), 143–156.
Tripathi, A. K.; Tsavalas, J. G.; Sundberg, D. C. Thermochim. Acta 2013, 568, 20–30.
Jiang, B.; Tsavalas, J.; Sundberg, D. Langmuir 2010, 26 (12), 9408–9415.
Jiang, B.; Tsavalas, J. G.; Sundberg, D. C. Prog. Org. Coatings 2017, 105, 56–66.
Chart: W𝑓nw for MMA-MA sample with and without SDS
| 1 | 3 | 5 | 7 | 9 | 11 | 13 | 15 | 17
MMA-MA ion-exchanged | 0 | 0.034179 | 0.035587 | 0.034649 | 0.036289 | 0.036172 | 0.03699 | 0.037263 | 0.038351
MMA-MA theoretical | 0.0376 | 0.0376 | 0.0376 | 0.0376 | 0.0376 | 0.0376 | 0.0376 | 0.0376 | 0.0376
MMA-MA with SDS | 0 | 0.059747 | 0.062203 | 0.063006 | 0.0627 | 0.062394 | 0.062203 | 0.06159 | 0.061513 | 0.061207
Cooling
Heating
Wet
Dry