## Slide 1: Composite Gelatin/Gelatin Methacryloyl Microgel-based Porous Hydrogel for Tissue Engineering Seth Edwards1, Shujie Hou1 and Kyung Jae Jeong* Department of Chemical Engineering, University of New Hampshire, Durham, NH 03824 1Equal Contributions *Corresponding author. Contact: KyungJae.Jeong@unh.edu
Previously, we reported an injectable macroporous hydrogel by crosslinking gelatin microgels by microbial transglutaminase (mTG) for use in wound healing. The method used to create this hydrogel was simple, requiring no chemical modifications to the starting reagents, cost-effective, and highly bio-functional, allowing for migration of cells into the hydrogel, and providing for optimal cell proliferation. However, despite displaying many advantageous qualities, this technology required a lengthy curing time (~ 60 minutes), limiting its usefulness in vivo. Using a similar methodology, a composite gelatin/gelatin methacryloyl (GelMA)-based injectable macroporous hydrogel that cures quickly, is minimally cytotoxic and stably adheres to the applied tissue was developed. This fast-curing hydrogel utilizes dual crosslinking; enzymatic crosslinking of gelatin by mTG, and photocrosslinking of GelMA by ultraviolet (UV) irradiation. Photocrosslinking achieves the initial rapid curing of microgels (< 2.5 minutes) to form a bulk macroporous hydrogel, while mTG strengthens the hydrogel by forming additional covalent crosslinks and allows the resulting hydrogel to adhere to the applied tissue.
Injectable hydrogels are of high interest for use as tissue engineering substrates. Factors paramount for clinical relevance for an injectable hydrogel system in this aim include gelation time, biocompatibility, tissue adhesion, and biodegradability. Herein these factors are examined for a novel injectable macroporous hydrogel assembled from gelatin/gelatin methacryloyl (gelMA) composite microgels. The use of multiple crosslinking mechanisms, namely microbial Transglutaminase (mTG), and ultraviolet (UV) irradiation to crosslink gelatin and gelMA respectively allowed for the optimization of photoinitiator concentration to minimize cell death upon UV irradiation. The result is a biodegradable hydrogel system that exhibited rapid gelation, optimized conditions for encapsulated cells, and capability for tissue adhesion, making it appropriate for use in tissue engineering applications.
Abstract
Conclusions
Rapid Curing of Composite Microgels
Live/Dead Assay on Encapsulated Cells: Z Projection
Research reported in this work was supported by NIH COBRE (CIBBR, P20 GM113131 to K.J.J.).
Rheological Characterization
Tissue Adhesion
Gelatin/GelMA Composite Microgels
Drastically decreased gelation time in comparison to gelatin macroporous hydrogel, enhancing clinical relevance
Dual crosslinking due to action of mTG and UV photocrosslinking allow for minimization of photoinitiator concentration, lowering cytotoxic effects from UV exposure.
Use of mTG allows for scaffold to adhere to surrounding tissue.
The presence of macropores allow for optimal growth and expansion of encapsulated cells, and infiltration of host tissue cells.
Day 7 Actin Cytoskeleton: Z Projection
Macroporous Hydrogel
Microgel
0.05% Photoinitiator
0.5% Photoinitiator
UV + mTG
UV Only
mTG Only
0.5% Photoinitiator
0.05% Photoinitiator
Nonporous
Red: Actin Cytoskeleton
Red: Dead Cells
Green: Living Cells
Day 7
Day 1
Conclusion: Use of both UV and mTG crosslinking allow for more rapid gelation
Experiment: Stable gelation was examined by allowing microgel suspensions to gel for 2.5 minutes under various conditions, and then submerged in a warm water bath (45 °C) to assess the formation of chemical crosslinks. Images were taken in a 12 well plate.
Experiment: Microgel suspensions were crosslinked in cavities made in porcine corneas by biopsy punches for 2.5 minutes. Corneas were then submerged in 45 °C to assess adhesion to corneal tissue.
Storage Modulus vs Time
Storage Modulus vs Temperature
Conclusion: Multiple crosslinking methods allow for minimization of photoinitiator concentration
UV Crosslinking Only
0.05 % Photoinitiator
0.5% Photoinitiator
mTG + UV Crosslinking
Conclusion: mTG, known widely as ‘meat glue’, was able to stable adhere rapidly formed hydrogel to corneal tissue.
100 µm
Acknowledgements
200 µm
200 µm
200 µm
200 µm
200 µm
200 µm
200 µm
0.05% Photoinitiator
0.5% Photoinitiator
Nonporous
200 µm
200 µm
200 µm
200 µm
200 µm
200 µm
100 µm