## Slide 1
Drift in Repeated Electrochemical Impedance Spectroscopy Measurements
Emily Ziino, Sabrina Marnoto, and Jeffrey M. Halpern
Chemical Engineering Department, University of New Hampshire
Using 1 mM FFCN
Threshold 370 ± 5% Ohms
Replacing buffer with deionized water
    Threshold: 21 ± 5% Ohms
Removing auxiliary and reference electrode
Removing working electrode
Acknowledgements: Our group would like to acknowledge the financial support of an Institutional Development Award (IDeA) from the National Institute of General Medical Sciences of the NIH under grant number P20GM113131, the Hamel Center of Undergraduate Research, and the Honors Program at the University of New Hampshire. We also recognize the support from the Surface Enhanced Electrochemical Diagnostic Sensors (SEEDS) Laboratory.
Problem and Approach
Future Work and Conclusion
Variables Tested
Chart: Z real (Ohms)
Glassy carbon working electrode
20 mM Fe3-/4-(CN)6 (FFCN) is used to promote electron transfer
Charge transfer resistance values increase with each run
AC Voltage: 5 mV
DC Voltage: 0 V vs Eoc
Experimental Technique Improvements
Cleaner surface – better polishing technique
  Rinse electrode with methanol and deionized water before and after polishing
Threshold: 19 ± 5% Ohms (18.05-19.95 Ohms)
Chart: Z real (Ohms)
Electrochemical Impedance Spectroscopy (EIS)
EIS is a common technique to evaluate surface state in batteries, biosensors, fuel cells
Drift and inconstant measurements can occur
We hypothesize that continued EIS runs increases the charging at the electrode surface and therefore decreases repeatability
Gamry Instruments. Basics of Electrochemical Impedance Spectroscopy. https://www.gamry.com/application-notes/EIS/basics-of-electrochemical-impedance-spectroscopy/ (accessed 11/7/2019).
Increasing Run #
Chart: Run
| 1 | 2 | 3 | 4 | 5 | 6
 | 18.8567 | 20.5033 | 21.8667 | 22.9967 | 24 | 24.8433
ΔRct: 6 Ohms
Chart: Run
| 1 | 2 | 3 | 4 | 5 | 6
 | 22.01 | 29.27 | 33.4267 | 36.34 | 38.6733 | 40.7067
Chart: Run
| 1 | 2 | 3 | 4 | 5 | 6
 | 18.8667 | 22.3833 | 24.2833 | 25.8133 | 27.2067 | 28.4833
Starting experiments with a cleaner working electrode surface decreased drift
Lower concentration of FFCN resulted in larger drift and error
Removing the reference and auxiliary electrodes increased drift
Removing the working electrode showed the least amount of drift
Replacing the buffer with deionized water showed the most drift
Future testing:
  Electrode type
  N2 purge of electrochemical cell
  Open circuit potential changes
  Double layer capacitance changes
Used Bode plots to display data which graph Zmod (Ohms) against Frequency (Hz) and Zphz (°) against Frequency (Hz)
Using 1 mM FFCN in PBS (Keeping All Electrodes) N=3
Deionized Water with 20 mM (Keeping All Electrodes) N=3
Remove Working Electrode (FFCN in PBS) N=3
Chart: Run
| 1 | 2 | 3 | 4 | 5 | 6
 | 371.5 | 500.8 | 576.7667 | 633.7333 | 681.5333 | 724.4
Chart: Run
| 1 | 2 | 3 | 4 | 5 | 6
 | 18.5733 | 21.8 | 24.23 | 26.51 | 28.65 | 30.09
ΔRct: 12 Ohms
Remove Auxiliary and Reference Electrode (FFCN in PBS) N=3
Chart: Frequency (Hz)
Chart: Frequency (Hz)
| 79453.13 | 63140.62 | 50203.12 | 39890.620000000003 | 31640.63 | 25171.88 | 20015.62 | 15890.62 | 12609.37 | 10078.129999999999 | 8015.625 | 6328.125 | 5015.625 | 3984.375 | 3170.9560000000001 | 2527.5729999999999 | 1976.1030000000001 | 1577.5239999999999 | 1265.625 | 998.26400000000001 | 796.875 | 627.79020000000003 | 505.5147 | 397.99529999999999 | 315.50479999999999 | 252.40379999999999 | 198.62289999999999 | 158.36150000000001 | 125.55800000000001 | 100.4464 | 79.002809999999997 | 63.3446 | 49.867019999999997 | 39.724580000000003 | 31.6723 | 24.933509999999998 | 19.862290000000002 | 15.83615 | 12.400790000000001 | 9.9311399999999992 | 7.9449149999999999 | 6.3173849999999998 | 5.008013 | 3.9457070000000001 | 3.158693 | 2.504006 | 1.9980819999999999 | 1.584686 | 1.2668919999999999 | 0.99904099999999996 | 0.79234280000000001 | 0.63344599999999995 | 0.50403229999999999 | 0.40064100000000002 | 0.31672299999999998 | 0.25201610000000002 | 0.20032050000000001 | 0.15889829999999999 | 0.12600810000000001 | 0.10016029999999999
Run 1 | 80.954 | 81.3625 | 81.8296 | 82.455 | 83.3547 | 84.4365 | 85.806 | 87.3722 | 89.0441 | 90.6059 | 91.9774 | 93.2716 | 94.2164 | 95.0288 | 95.6256 | 96.0851 | 96.4669 | 96.8081 | 97.0467 | 97.3312 | 97.5543 | 97.8549 | 98.1014 | 98.4163 | 98.7469 | 99.0747 | 99.4516 | 99.8673 | 100.3362 | 100.8461 | 101.4763 | 102.0808 | 102.8706 | 103.696 | 104.6042 | 105.7332 | 107.2048 | 108.4907 | 110.1309 | 111.6909 | 113.5928 | 115.7246 | 118.2328 | 121.1547 | 124.1932 | 127.7298 | 131.6966 | 136.2698 | 141.2151 | 147.3089 | 153.9586 | 161.1597 | 169.513 | 178.9993 | 189.9339 | 202.0875 | 215.7646 | 231.45 | 249.4078 | 269.3822
Run 2 | 79.8267 | 80.2393 | 80.8059 | 81.5167 | 82.5167 | 83.7005 | 85.2452 | 87.0045 | 88.8996 | 90.8274 | 92.6453 | 94.3428 | 95.6685 | 96.7673 | 97.6037 | 98.3171 | 98.865 | 99.3252 | 99.6015 | 99.9575 | 100.2346 | 100.5887 | 100.8713 | 101.1801 | 101.5189 | 101.8497 | 102.2414 | 102.651 | 103.1261 | 103.6266 | 104.2329 | 104.8281 | 105.5923 | 106.3963 | 107.289 | 108.3509 | 109.8132 | 111.0642 | 112.6548 | 114.1535 | 116.0053 | 118.057 | 120.5178 | 123.3427 | 126.3287 | 129.7937 | 133.6923 | 138.1992 | 143.09 | 149.1269 | 155.7007 | 162.8731 | 171.1543 | 180.6095 | 191.6318 | 203.695 | 217.4474 | 233.078 | 251.1015 | 271.3874
Run 3 | 79.7672 | 80.1745 | 80.6842 | 81.3978 | 82.3817 | 83.6019 | 85.101 | 86.9389 | 88.9775 | 91.0811 | 93.0867 | 95.0336 | 96.6672 | 97.9727 | 98.9644 | 99.78 | 100.3954 | 100.9012 | 101.3067 | 101.6865 | 102.0213 | 102.3373 | 102.6461 | 102.9714 | 103.298 | 103.6326 | 104.0612 | 104.4892 | 104.954 | 105.441 | 106.0461 | 106.667 | 107.4055 | 108.1986 | 109.0873 | 110.157 | 111.549 | 112.8382 | 114.3897 | 115.9387 | 117.7674 | 119.8208 | 122.2944 | 125.0933 | 128.0619 | 131.5208 | 135.3908 | 139.8848 | 144.7982 | 150.7996 | 157.3295 | 164.4973 | 172.7641 | 182.2393 | 193.2383 | 205.2632 | 218.9416 | 234.5811 | 252.552 | 272.8221
Run 4 | 79.8186 | 80.1973 | 80.7123 | 81.4324 | 82.3639 | 83.5722 | 85.1264 | 86.9966 | 89.1094 | 91.3465 | 93.5617 | 95.6927 | 97.4654 | 98.9311 | 100.0777 | 101.0131 | 101.7416 | 102.285 | 102.7545 | 103.0954 | 103.4775 | 103.8078 | 104.1115 | 104.4451 | 104.775 | 105.1167 | 105.5261 | 105.9318 | 106.4225 | 106.9201 | 107.5123 | 108.1197 | 108.8827 | 109.6574 | 110.5923 | 111.5877 | 113.021 | 114.2027 | 115.773 | 117.3113 | 119.2018 | 121.308 | 123.7098 | 126.5051 | 129.4892 | 132.9353 | 136.8107 | 141.2925 | 146.1859 | 152.0825 | 158.7025 | 165.8708 | 174.0918 | 183.5204 | 194.4274 | 206.4795 | 220.1487 | 235.735 | 253.703 | 273.9123
Run 5 | 79.7536 | 80.1423 | 80.6544 | 81.3748 | 82.3096 | 83.4867 | 85.0286 | 86.9294 | 89.1246 | 91.4279 | 93.8115 | 96.1008 | 98.0734 | 99.6518 | 100.934 | 101.9937 | 102.7516 | 103.3451 | 103.8788 | 104.3153 | 104.6334 | 105.0158 | 105.3484 | 105.6996 | 106.0314 | 106.3748 | 106.7755 | 107.1934 | 107.6813 | 108.1769 | 108.7702 | 109.3893 | 110.1311 | 110.9216 | 111.7884 | 112.8609 | 114.3169 | 115.5401 | 117.1066 | 118.6167 | 120.5006 | 122.5735 | 124.9612 | 127.7508 | 130.698 | 134.1481 | 138.0059 | 142.5043 | 147.3618 | 153.3492 | 159.8624 | 166.9777 | 175.1995 | 184.6344 | 195.5596 | 207.5335 | 221.1964 | 236.7581 | 254.6353 | 274.5356
Run 6 | 79.7709 | 80.1664 | 80.6845 | 81.3684 | 82.3094 | 83.4718 | 85.0139 | 86.9406 | 89.1832 | 91.5605 | 94.0775 | 96.4795 | 98.6359 | 100.3825 | 101.7836 | 102.869 | 103.8059 | 104.4339 | 104.9449 | 105.4194 | 105.8097 | 106.1734 | 106.4831 | 106.8389 | 107.1934 | 107.5303 | 107.9384 | 108.3739 | 108.8361 | 109.3332 | 109.9496 | 110.5695 | 111.3064 | 112.1149 | 112.9794 | 114.0351 | 115.4197 | 116.7088 | 118.2377 | 119.8201 | 121.6499 | 123.6729 | 126.0909 | 128.8879 | 131.834 | 135.2566 | 139.1326 | 143.5828 | 148.4599 | 154.4163 | 160.94 | 168.061 | 176.2842 | 185.696 | 196.5755 | 208.5643 | 222.0615 | 237.658 | 255.5551 | 275.7325
Run 1 | -2.9326 | -3.2475 | -3.5999 | -4.0439 | -4.4969 | -4.8817 | -5.1799 | -5.3266 | -5.3172 | -5.0892 | -4.7459 | -4.2768 | -3.8137 | -3.3692 | -2.9586 | -2.6393 | -2.339 | -2.1066 | -1.9671 | -1.8475 | -1.7865 | -1.753 | -1.7536 | -1.8077 | -1.8884 | -1.9968 | -2.1343 | -2.3068 | -2.5044 | -2.7318 | -3.0068 | -3.2992 | -3.6505 | -4.0285 | -4.4313 | -4.918 | -5.4151 | -5.9643 | -6.6137 | -7.2832 | -7.9803 | -8.7632 | -9.614 | -10.5556 | -11.4884 | -12.4347 | -13.5081 | -14.668 | -15.826 | -17.0889 | -18.3626 | -19.6206 | -20.909 | -22.216 | -23.533 | -24.7993 | -26.0596 | -27.2835 | -28.486 | -29.6193
Run 2 | -3.1223 | -3.4569 | -3.8492 | -4.3334 | -4.8526 | -5.3482 | -5.769 | -6.0421 | -6.1249 | -6.0009 | -5.6538 | -5.164 | -4.6228 | -4.055 | -3.5717 | -3.1228 | -2.7367 | -2.4599 | -2.2094 | -2.0211 | -1.8934 | -1.83 | -1.8027 | -1.8093 | -1.8532 | -1.9357 | -2.0536 | -2.1945 | -2.3735 | -2.5734 | -2.8269 | -3.1029 | -3.426 | -3.7775 | -4.1764 | -4.6204 | -5.0844 | -5.6106 | -6.2574 | -6.8769 | -7.5626 | -8.3247 | -9.1535 | -10.0696 | -10.9877 | -11.9143 | -12.9786 | -14.1365 | -15.2914 | -16.5565 | -17.8415 | -19.1106 | -20.4212 | -21.7483 | -23.1013 | -24.4059 | -25.6977 | -26.9559 | -28.188 | -29.3598
Run 3 | -3.1953 | -3.4982 | -3.9394 | -4.4349 | -4.9982 | -5.5522 | -6.0585 | -6.4302 | -6.5963 | -6.5486 | -6.2654 | -5.7741 | -5.1955 | -4.5783 | -4.0209 | -3.5259 | -3.0423 | -2.7006 | -2.4111 | -2.1962 | -2.0223 | -1.9333 | -1.8781 | -1.8594 | -1.8959 | -1.9499 | -2.0562 | -2.1873 | -2.3506 | -2.5515 | -2.8008 | -3.0586 | -3.3725 | -3.7124 | -4.1103 | -4.5388 | -5.0048 | -5.534 | -6.1494 | -6.7662 | -7.4423 | -8.1891 | -9.0137 | -9.9166 | -10.8302 | -11.7492 | -12.8101 | -13.9487 | -15.1026 | -16.366 | -17.6485 | -18.9046 | -20.2228 | -21.552 | -22.9037 | -24.2101 | -25.5028 | -26.764 | -28.0088 | -29.1913
Run 4 | -3.2131 | -3.5573 | -4 | -4.4965 | -5.0777 | -5.6984 | -6.2401 | -6.6845 | -6.9246 | -6.9224 | -6.6809 | -6.2079 | -5.6274 | -4.988 | -4.3958 | -3.8127 | -3.2987 | -2.9069 | -2.5934 | -2.3347 | -2.1376 | -2.0098 | -1.9433 | -1.9144 | -1.9219 | -1.9745 | -2.0653 | -2.1872 | -2.344 | -2.5353 | -2.7721 | -3.02 | -3.3454 | -3.6686 | -4.0461 | -4.4792 | -4.9477 | -5.455 | -6.071 | -6.6856 | -7.3511 | -8.0906 | -8.9032 | -9.8046 | -10.7054 | -11.6115 | -12.6689 | -13.8028 | -14.9457 | -16.2077 | -17.4738 | -18.7394 | -20.0495 | -21.376 | -22.7329 | -24.0404 | -25.3407 | -26.6091 | -27.8508 | -29.0462
Run 5 | -3.2483 | -3.5873 | -4.0188 | -4.5812 | -5.1684 | -5.8116 | -6.4133 | -6.9004 | -7.2155 | -7.2512 | -7.0737 | -6.6153 | -6.0125 | -5.3588 | -4.6973 | -4.0988 | -3.5299 | -3.0902 | -2.7592 | -2.463 | -2.2531 | -2.092 | -2.0112 | -1.9536 | -1.954 | -1.9959 | -2.0772 | -2.1894 | -2.3417 | -2.5231 | -2.7469 | -2.9946 | -3.3083 | -3.6329 | -4.0048 | -4.4193 | -4.8747 | -5.3825 | -5.9909 | -6.6076 | -7.2564 | -7.9983 | -8.8019 | -9.6956 | -10.593 | -11.4965 | -12.5399 | -13.665 | -14.8072 | -16.0588 | -17.3291 | -18.5879 | -19.8986 | -21.2189 | -22.5774 | -23.8921 | -25.1921 | -26.4605 | -27.7172 | -28.8876
Run 6 | -3.2766 | -3.6165 | -4.0768 | -4.5969 | -5.2502 | -5.8895 | -6.5231 | -7.0964 | -7.4552 | -7.5715 | -7.3886 | -6.9768 | -6.3674 | -5.6832 | -5.0053 | -4.3825 | -3.749 | -3.2822 | -2.9238 | -2.581 | -2.3375 | -2.1792 | -2.0692 | -2.0005 | -1.9873 | -2.0125 | -2.0877 | -2.1931 | -2.3319 | -2.5015 | -2.7328 | -2.973 | -3.2703 | -3.5973 | -3.9512 | -4.404 | -4.835 | -5.3214 | -5.9353 | -6.537 | -7.1895 | -7.9186 | -8.7104 | -9.6022 | -10.488 | -11.3872 | -12.4293 | -13.5515 | -14.6858 | -15.9306 | -17.2028 | -18.457 | -19.7554 | -21.0756 | -22.4372 | -23.7523 | -25.058 | -26.3333 | -27.5897 | -28.7813
Chart: Frequency (Hz)
Chart: Frequency (Hz)
Chart: Frequency (Hz)
Notes: Reproducibility issues arise with repeated measurements using EIS
Charge transfer resistance values increase with each run
Could do 1mM FFCN or list out 6 rct values from over the summer