## Slide 1: Gelatin-Based Microporous Hydrogel for Injectable Cell Delivery Seth Edwards, Kyung Jae Jeong* Department of Chemical Engineering, University of New Hampshire, Durham, NH 03824 *Corresponding Author Contact: KyungJae.Jeong@unh.edu
Accelerated Tissue Regeneration
Cell delivery is a promising technology to enhance treatment of tissue repair. Cell retention and survival at the site of injection is poor for direct injection of cells. Injectable hydrogels can provide a scaffold to retain delivered cells at the injection site, and serve as a scaffold to facilitate tissue repair. Gelatin microgels are created through a water-in-oil emulsion. Microgels are annealed to each other by an enzymatic crosslinking process, and cells are encapsulated in the interstitial space between microgels.
Microgels can be injected, and clearly show a microporous structure under SEM, with pores formed in the interstitial space between microgels.
We examined the use of gelatin-based microporous hydrogel for in situ cell encapsulation of mesenchymal stem cells (MSCs) and neural stem cells (NSCs) for applications in bone repair, anti-inflammatory therapy, and neural tissue repair. The advantage of this approach is that microporous hydrogel facilitates cell spreading and cell-cell connections which are important in promoting cell behaviors such as MSC osteogenic differentiation and neuronal differentiation of NSCs.
Neural Stem Cell (NSC) Delivery for Neural Regeneration
Mesenchymal Stem Cell Delivery for Bone Repair
MSCs encapsulated in the microporous hydrogel were able to undergo morphological changes due to osteogenic differentiation, in comparison to the nonporous hydrogel where cells were trapped in the gel mesh.
Increased MSC osteogenic differentiation was seen for cells grown in the microporous hydrogel, by ALP staining and assay, calcium deposition, and ALP/BGLAP gene expression.
MSCs primed by IFN-γ released more anti-inflammatory molecules when encapsulated in the microporous hydrogel than the nonporous analog.
Neural stem cells form cell clusters and display elongated connections to other cells, demonstrating neuronal differentiation by staining of differentiation factor Tuj1.
Introduction
Conclusions
Acknowledgements
Mesenchymal Stem Cell Delivery for Anti-inflammatory Effects
Day 14 Alkaline Phosphatase (ALP) Staining
ALP is a marker for osteogenic differentiation. We saw improved staining of ALP in microporous hydrogel compared to a nonporous alternative when cells were supplemented with osteogenic differentiation factors.
Quantitative Assessment of Osteogenic Differentiation
MSC Encapsulation: Cell Growth
MSCs spread and rapidly proliferate in the microporous hydrogel in comparison to the nonporous analog.
Anti-inflammatory Cytokine Release
Optimization of Neural Stem Cell Seeding Density
Optimization of Cell Seeding:
Neural stem cell seeding density is highly important for cell survival and proliferation. Cells seeded at higher densities survived and showed higher proliferation in the hydrogel.
Neuronal Differentiation of NSCs in the Microporous Hydrogel
I would like to acknowledge my PI Dr. Kyung Jae Jeong, collaborator Dr. Young Jo Kim, current and prior students in our lab, the UNH UIC for their help with imaging and characterization, the UNH Department of Chemical Engineering for supporting me through a teaching assistantship, and funding sources NIH COBRE (CIBBR, P20 GM113131), and NSF NH Biomade.
Microporous Hydrogel
Injectability
Live/Dead
Porous
Nonporous
1 Million Cells/mL
3 Million Cells/mL
6 Million Cells/mL
Day 14: Growth
Day 14: Differentiation
Porous
Nonporous
Live/Dead
50 um
50 um
50 um
50 um
MSC Morphology Changes When Exposed to Differentiation Factors
IL-6 Release
Prostaglandin E2 (PGE2) Release
Red: ALP Staining
Nonporous
Porous
200 um
1 mm
1 mm
200 um
ALP Activity
ALP Gene Expression
Osteocalcin Gene Expression
100 um
200 um
Neuronal Differentiation of NSCs in the Microporous Hydrogel:
When given factors for neuronal differentiation, neural stem cells cluster and form elongated connections to other cells. Beta-Tubulin III (Tuj1) is a marker of neurons.
Blue: Cell Nuclei
Green: Tuj1
Red: Actin Cytoskeleton
Day 1
Day 7
200 um
200 um
200 um
200 um
Low magnification: Z Projection and 3D View
High magnification: Z Projection and 3D View
Calcium Deposition
Mesenchymal stem cells were primed with IFN-γ before encapsulation. Release of anti-inflammatory cytokines was measured, and cells encapsulated in the porous hydrogel showed greater cytokine release in comparison to the nonporous alternative.